## Slide 1
Online conference presentation
17-28 May 2021
8th International Symposium on Sensor Science
Self-assembled monolayers based on 1,3-dimercaptopropan-2-ol: preparation, characterization and applications in electrochemical chemosensors

## Slide 2
2
Context and objectives
Investigation on modified electrodes in electroanalytical applications
Many approaches have been used:
Molecular self assembly (SAM)
Work topic ?
Why SAMs are important?
They provide grafting of monolayers and also multilayers of 3D molecular structures onto an electrode surface
What does SAMs mean?
Metal Substate
Terminal functional group
Spacer (AlkaneChain)
Ligand or head group

## Slide 3
3
Context and objectives
SAMs are widely applied in sensing and biosensing.
Lack of stability
Lack of reproducibility
Non specific response
SAM properties
Simplicity of preparation
Ability to transfer optical / electrical properties
Introducing chemical funtionalities
Ability to link macroscopic phenomena of the interface

## Slide 4
4
Context and objectives
How can we overcome these limitations?
The mostly known example: thiotic acid
Use anchor molecules possessing more than one thiol moieties
1,3-dithioacetatepropan-2-ol
Symmetrical structure
Better orientation of the tethered structures
High stability
Contains two thiol groups protected by acetate

## Slide 5
5
Electrochemical investigation of the anchor site
Immobilization fashion of the 1,3-dimercaptopropan-2-ol onto gold substrate
3 h / 0.1 M
SAM 1
SAM 2
12 h / 1 mM

## Slide 6
6
Electrochemical investigation of the anchor site
Electrodes | CV in K3[Fe (CN)6] 10 Mm |  |  | 
 | ΔEp (mV) | Ip,a (µA) | A / A0 | k0 (ms-1)
Bare gold | 115 ± 2 | 1040.2 ± 0.1 | 1 | (3.05 ± 0.67)10-5
SAM1 | 308 ± 7 | 722.5 ± 0.4 | 0.569 | (0.52 ± 0.03)10-5
SAM2 | 160 ± 5 | 774 ± 1 | 0.827 | (1.93 ± 0.62)10-5
Uncoated gold
SAM1
SAM2
Randles-Sevcik plots
Cyclic voltammograms in:
10 mM K4[Fe(CN)6] + 0.1 M KCl
at different sweep rates

## Slide 7
7
Electrochemical investigation of the anchor site
Michael addition
No binding
Binding
Cyclic voltammograms recorded in phosphate buffered saline (PBS) at pH = 7.4 after 40 min incubation in 5mM ethanolic solution of BQ

## Slide 8
8
Spectroscopic investigation of the anchor site

## Slide 9
9
Spectroscopic investigation of the anchor site
SAM 1
30 %
70 %
SAM 2
70 %
30 %

## Slide 10
10
Electrochemically active SAM design
A. Laroussi, M. Kot, J. Ingo Flege, N. Raouafi, V. M. Mirsky, Appl. Surf. Sci. 2020, 513, 145827.

## Slide 11
12
Electrocatalytic sensing of hydrogen peroxide
Calibration Curve
LOD : 2,3 μM
Sensitivity : 1700 A.m-2.L.mol-1
Chronoamperometry responses for successive hydrogen peroxide additions
Gold modified SAM-terminated-BQ
E = + 0.4 V (vs. Ag/AgCl)

## Slide 12
13
Electrocatalytic sensing of hydrogen peroxide
Fast response
High sensitivity
No interferents
Test of selectivity
H2O2
(3 mM)
Glucose (7 mM)
Uric Acid (0.36 mM)
Ascorbic Acid (0.1 mM)
Glucose (14 mM)
Uric Acid (0.72 mM)
Ascorbic Acid (0.2 mM)
H2O2 (4 mM)
A. Laroussi, N. Raouafi, V. M. Mirsky, Electroanalysis (minor correction)

## Slide 13
18
https://doi.org/10.1016/j.talanta.2018.11.026
To conclude !
Preparation and characterization of SAMs based on the symmetric molecule with two thiol groups
Electrochemically active SAM terminated-BQ
Application of this system for hydrogen peroxide analysis in different technological processes
BQ is a perspective material for the development of electrocatalytic sensors for hydrogen peroxide

## Slide 14
Thanks for your attention !