## Slide 1: Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
Dipartimento di Chimica
E. Pargoletti1,2*, A. Tricoli3, M. Longhi1,2, G. L. Chiarello1 and G. Cappelletti1,2
1 Dipartimento di Chimica, Università degli Studi di Milano, via Golgi 19, 20133, Milano, Italy
2 Consorzio Interuniversitario Nazionale per la Scienza e Tecnologia dei Materiali (INSTM), Via Giusti 9, 50121, Firenze, Italy
3 Nanotechnology Research Laboratory, Research School of Engineering, Australian National University, Canberra 2601, Australia
e-mail: eleonora.pargoletti@unimi.it
NRL
Nanotechnology Research Laboratory

## Slide 2
Introduction: VOCs Sensing
Why and How
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it
Light-assisted sensing
Inexpensive
Portable
Accurate
Low LOD
Gas Sensors
Meng et al., Trends Anal. Chem., 37 (2015) 37–47
Tricoli et al., Adv. Funct. Mater., (2017) 1605271
2/10

## Slide 3
Introduction: VOCs Sensing
Why and How
Light-assisted sensing
Hyo-Joong Kim et al., Sensors and Actuators B, 192 (2014) 607–627
Metal Oxide
Hybrid
chemoresistor
M. Arvani et al., Sci. Iran., 3 (2017) 3033
2/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 4
Gas in
Gas out
20 ppm
10 ppm
4 ppm
2 ppm
1 ppm
0.8 ppm
0.6 ppm
0.4 ppm
0.2 ppm
Kim et al., ACS Appl. Mater. Interfaces, 7 (2015) 17199−17208
Analyzed biomarkers
Ethanol: alcohol misuse
Acetone: diabetes type I
Toluene/ethylbenzene: lung cancer
Complexity
Medical applications
Sensitivity & Selectivity
Operating T = 300 °C
Light assisted-low operating T sensing
Synthesis of metal oxide (MOS) / graphene oxide (GO) nano-heterojunctions:
increased conductivity under light sources, reducing the OT
synergistic effect between MOS and GO
Response and Recovery Times
A General Overview
3/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it
Different Metal Oxide Semiconductors (MOS)
ZnO
SnO2
WO3
SnO2-TiO2
Notes: Composite materials/mixed oxides

## Slide 5
H2SO4, NaNO3, KMnO4
H2O2 (30 %wt)
Modified Hummers method
Graphene Oxide (GO)
Powder graphite (G)
Graphene oxide (GO) synthesis
Pure MOS
GO aqueous suspension
(3.0 mg mL-1)
Different MOS salt/GO weight ratios (i.e. 4 – 32)
MOS salt precursors (Zn(NO3)2, SnCl4, Na2WO4, H2WO4, TTPI)
400oC, 6 h
O2
50 oC, 6 h
Pure MOS
Precipitating/structure directing agents
(NH4OH, urea, oxalic acid, tensides, NaOH)
MOS-GO
MOS NPs
Pargoletti* et al., Nanomaterials, 10 (2020) 761
MOS-GO nano-heterojunctions
The Adopted Synthetic Route
Pargoletti et al., ACS Appl. Mater. Interfaces, 12 (2020) 39549−39560
4/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it
Pargoletti* et al., Applied Surface Science, 483 (2019) 1081–1089
Pargoletti et al., Nanoscale, 11 (2019) 22932-22945
Notes: Depending on the material

## Slide 6
Materials Physico-Chemical Characterizations
The case of SnO2 and SnO2/GO
SnO2
4:1 SnO2/GO
32:1 SnO2/GO
XRPD
Raman
XPS
Sample | SBET (m2 g-1) | Vtot. pores (cm3 g-1)
Graphite | 11 | 0.030
GO | 30 | 0.010
SnO2 | 67 | 0.210
4:1 SnO2/GO | 40 | 0.110
32:1 SnO2/GO | 50 | 0.133
5/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 7
Electrode
Flowmeters
Sensing chamber
Gas inlet/outlet
Lamp: UV Thorlabs
(290 - 370 nm, 2-20 W cm-2)
Heating controller
Potentiostat/Galvanostat, applied bias = +1.0 V
Valves
Heating plate
4 mL of ethanol powders suspensions (2.5 mg mL-1) sprayed (p = 0.8 bar) on a heating plate (230 oC)
 Final calcination step (in air, at 350 oC for 1 h)
Range 2-5 𝝻m
Tips
Gas Sensing Set-Up
Sensing layer deposition
6/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 8
ZnO-based materials
RT sensing
RT sensing
With the highest GO coverage by MOS NPs (32:1 MOS/GO), 100 ppb of ethanol are sensed at RT with the aid of UV light
By comparing ZnO-based to SnO2-based materials: tin dioxide matrix gives the greatest response signal, both at high and low T
Pargoletti et al., Nanoscale, 11 (2019) 22932-22945
Gas Sensing
Sensitivity at high and low T (UV-aided) – The case of hybrid 32:1 ZnO/GO and SnO2/GO towards EtOH
OT = 150 °C
ZnO
32:1 ZnO/GO
OT = 350 °C
UV off
OT = 350 °C
UV off
SnO2-based materials
Pargoletti, Hossain, Di Bernardo, Chen, Tran-Phu, Lipton-Duffin, Chiarello, Cappelletti, Tricoli, ACS App. Mat.&Int., 12 (2020) 39549−39560
Pargoletti* et al., Applied Surface Science, 483 (2019) 1081–1089
SnO2
32:1 SnO2/GO
OT = 350 °C
UV off
OT = 350 °C
UV off
OT = 150 °C
7/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 9
Increasing of Ti content
Gas Sensing
Selectivity – The case of ternary hybrid 32:1 SnO2-TiO2/GO towards Acetone and Toluene
4 ppm of VOCs, 350 oC
LOD 0.1-0.2 ppm
At high T, 32:1 SnO2/GO has higher selectivity towards acetone than toluene
At high T, Sn0.55Ti0.45/GO is the most selective to toluene
At lower T, with UV light: Sn0.55Ti0.45/GO keeps the selectivity towards toluene molecules
Eg = 3.26
Eg = 3.20
Eg = 3.40
4 ppm of VOCs, 250 oC
8/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 10
n-type oxide semiconductor sensing mechanism
H.J. Kim et al., Sensors and Actuators B, 192 (2014) 607–627
H.W. Kim et al., Sensors and Actuators B, 249 (2017) 590–601
O2(gas) → 2O(ads)
O(ads) + e-(from MO) → O2-(ads) RT < T < 100 °C
O2-(ads) + e- → 2O-(ads) 100 < T < 300 °C
O-(ads) + e- → O2-(ads) T > 300°C
Reducing gas + ads oxygen species → CO2 + e-(to MO) (R decreases)
The Hypothesized Mechanism
Reaction
Simple ads
WO3
9/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 11
n-type oxide semiconductor sensing mechanism
O2(gas) → 2O(ads)
O(ads) + e-(from MO) → O2-(ads) RT < T < 100 °C
O2-(ads) + e- → 2O-(ads) 100 < T < 300 °C
O-(ads) + e- → O2-(ads) T > 300°C
Reducing gas + ads oxygen species → CO2 + e-(to MO) (R decrease)
Band structure of (a) only hydroxyl GO and (b) only epoxy GO
H. Luo et al., J. Appl. Phys., 122 (2017)
p(GO)-n(MOS)
nano-heterojunctions
The Hypothesized Mechanism
Photocurrent measurements
Pargoletti et al., Nanoscale, 11 (2019) 22932-22945
9/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 12
Conclusions
32:1 SnO2/GO: highly selective to EtOH
32:1 SnxTi1-x/GO samples: higher selectivity to toluene
4:1 SnO2/GO: much more selective to EtBz, displaying a reversed signal
Pivotal role of GO and UV light
p-n heterojunction in hybrid materials
high performances of composites also as photodetectors
Fundamental role of pores shape/size, specific surface area
films with thickness < 5 μm
Sensitivity
SnO2 is the most performing matrix showing the highest intensity response
low LOD values (of 100 ppb) are reached even at RT
Selectivity
Light assisted-low operating T sensing
Sensor & possible mechanism
Response and
Recovery Times
10/10
Disclosing the Sensitivity and Selectivity of Metal Oxide/Graphene Oxide-based Chemoresistors Towards VOCs
e-mail: eleonora.pargoletti@unimi.it

## Slide 13
Thank you for your kind attention!
NRL
Nanotechnology Research Laboratory