## Slide 1: Evaluation of the parameters of poly(butylene succinate) enzymatic polymerization C. I. Gkountela, D. N. Markoulakis, D. M. Korres, S. N. Vouyiouka* Laboratory of Polymer Technology, School of Chemical Engineering, National Technical University of Athens, Greece, (*mvuyiuka@central.ntua.gr)
Introduction
Poly(butylene succinate) (PBS) is a bio-based and biodegradable polyester, that can be used in numerous applications, especially in the biomedical sector [1,2]. Even though green polymerization routes such as biocatalysis are being developed [3,4], there is a very limited literature on the enzymatic synthesis of PBS and in most of the works where high-molecular-weight PBS is produced, several drawbacks may impede the process scaling up. On that basis, an eco-friendly, solvent-free, enzyme-based process for the production of PBS was applied and the most important process parameters were evaluated.
Experimental part
Figure 2. Enzymatically synthesized PBS oligomer (scaled up,10 g)
Figure 1. Apparatus for the production of PBS oligomers
References
Results and Discussion
Figure 3. of the enzymatically synthesized oligomers
Figure 4. and Tm of the enzymatically synthesized oligomers
The synthesized at 90 °C, 20 mbar, 2h product was successfully scaled up (ca. 10 g of product).
(g/mol) | (g/mol) | Tm1 (°C) | Tc (°C) | Tm2 (°C) | Td,5% (°C) | Td (°C) | Residue (%)
1000 | 4700 | 104 | 57 | 103 | 258 | 387 | 1,44
 |  | Tm1 (°C) | Tc (°C) | Tm2 (°C) | Td,5% (°C) | Td (°C) | Residue (%)
1000 | 4700 | 104 | 57 | 103 | 258 | 387 | 1,44
Conclusions
The bulk enzymatic polymerization route resulted in a PBS grade of 4700 g/mol, crystallinity ca. 61% and melting points at ca. 104°C. This free of thermal degradation and metal catalyst residues grade is appropriate to be used in biomedicine applications where low controlled molecular weight is usually needed.
[1] Xu J, Guo B.H, Biotechnology Journal. 2010; 1149–1163.
[2] Gigli M, Fabbri M, Lotti N, Gamberini R, Rimini B, Munari A. European Polymer Journal. 2016; 75: 431–460.
[3] Douka A, Vouyiouka S, Papaspyridi L.M, Papaspyrides C.D. Progress in Polymer Science. 2018; 79: 1–25.
[4] Gkountela C, Rigopoulou M, Barampouti E.M, Vouyiouka S. European Polymer Journal. 2021; 143: 110197
Table 1. Scaled-up PBS oligomer’s properties
N435
Reaction: 40℃, 24h (1st stage)
Reaction: T , P , t2 (2nd stage))
CHCl3
Filtration, Drying
Optimum conditions: 90°C, 20 mbar, 2h
Reaction temperature
Pressure
Reaction time
Evaluated process parameters:
90 and 95°C
at 90°C, at 95°C
at 90°C and 95°C
1,4 BDO DES
PBS + N435
PBS + N435
PBS + N435
PBS oligomer