## Slide 1
Comparison of Optoelectronic Properties of Doped and Pristine Nanotubes Based on Carbon and Tungsten Disulfide
Maksim Paukov, Anastasia Goldt, Gennadiy Komandin, Alexander Syuy, Dmitriy Yakubovskiy, Sergei Novikov, Alexander Polyakov, Reshef Tenne, Alla Zak, Albert Nasibulin, Aleksei Arsenin, Valentyn Volkov, Maria Burdanova
e-mail: paukov.mi@phystech.edu
Introduction
Aim: investigation of the optical and terahertz features of carbon (C) and tungsten disulfide (WS2) nanotubes (NT) and tuning of these properties by p-type doping with HAuCl4 (gold nanoparticles)
Approach: geometry of given samples was studied by transmission and scanning electron microscopy (TEM and SEM respectively), their optoelectronic features were examined via Raman spectroscopy, absorption spectroscopy in ultra-violet and visible range, and terahertz spectroscopy in time domain (TDS).
Sample preparation
Organic and inorganic Nanotubes
Optical properties
Terahertz spectroscopy
Future plans
Acknowledgements
References
Both CNTs and WS2NTs are theoretically constructed by rolling up a 2D sheet of the corresponding material to form a single-walled or multi-walled cylinder (Fig. 1).
Regardless of the production method, 2/3 of obtained CNTs demonstrate metallic behavior and 1/3 - semiconducting, whereas WS2NTs are semiconducting ones.
P-doping shifts the Fermi level of the materials, allowing to control their optoelectronic properties.
CNTs films were synthesized using the aerosol method
WS2NTs films were produced from commercially-available powder (NanoMaterials Ltd) using vacuum filtration method
When the energy of incident photons matches these transitions the resonant enhancement of photophysical processes such Raman scattering, Absorption, and others are expected to be seen.
Fig. 2. TEM images of a) CNTs (blue arrows show the bundles, small particles are catalysts) and b) typical individual WS2NT (the orange line shows the diameter, light green arrows - the thickness of NT’s walls); c) SEM image of doped WS2NT (yellow arrows indicated NT dotted with gold nanoparticles, green arrow shows the typical length).
This project is supported by Russian Science Foundation (No. 21-79-10097), Ministry of Science and Higher Education of the Russian Federation (No. 075-15-2021-606), and Russian Foundation for Basic Research (No.18-29-27010 MK).
The absorption spectroscopy allowed us to detect the excitonic transitions in the NT as well as the impact of p-doping on shifting the Fermi level. Compare to their 2D analogues, NTs demonstrate a shift in the position of these transitions.
Both types of NTs appear to have two contributions in their conductivity: 1) a Drude component, responsible for the motion of free charges in the presence of the electric field; 2) a Lorentz component, which describes the localized state of axial plasmons.
Fig. 3. Raman spectra of CNT (right) and WS2NT (left).
Fig.4. Absorbance spectra of CNT (left) and WS2NT (right).
Fig.5. Terahertz conductivity of CNT(top) and WS2NT(bottom).
Different length and diameter WS2NT with different morphology are to be investigated to understand the origin of the conductivity peak in THz region.
Microscopy characterization
The morphology of studied samples was investigated using TEM and SEM.
The TEM images showed that CNTs tend to form bundles due to the interactions via Van der Waals forces. The averaged diameter of the bundle was 8.9 nm while the mean diameter of individual NT - 1.8 nm. The averaged length is >10 μm.
WS2NTs appear to be multi-walled and have a wider diameter distribution of 79.6 nm. The SEM images allowed to determine the mean length of WS2NTs, which is 1.3 µm.
Fig. 1. The scheme of tubes’ formation.
As it can be seen, the p-doping influences the position and lessens the intensity of Raman active modes. Compared to their 2D-counterparts, the NT show a difference of the resonant frequencies, which can be explained by the strain and curvature of the tube’s structure. Doping with HAuCl4 results in the shift towards higher frequency in both CNT and WS2 NT which indicates p-doping.
The peak, corresponding to axial plasmon, is red-shifted for WS2NTs compared with CNTs due to the difference in the length. Doping leads to the broadening of the conductivity due to the additional free charges.
Overall, NT possesses the optoelectronic properties that are changed because of the curvature, quantum confinement, and localization. Doping with HAuCl4 results in tunability of all optoelectronic properties.
Conclusions
Burdanova M. G., et.al., A Review of the Terahertz Conductivity and Photoconductivity of Carbon Nanotubes and Heteronanotubes. Adv. Optical Mater., 2021, 210104.
Sinha S.S., et. al., MoS2 and WS2 Nanotubes: Synthesis, Structural Elucidation, and Optical Characterization. J. Phys. Chem. C, 2021, 125 (11), 6324-6340.