## Slide 1
Anna Lysova1, I.I. Ponomarev2
1Kurnakov Institute of General and Inorganic Chemistry RAS, Moscow, Russia
2Nesmeyanov Institute of Organoelement Compounds RAS, Moscow, Russia
* ailyina@yandex.ru, www.igic.ras.ru
Disadvantages of PBI
                acid leaching from membrane matrix
material corrosion in the presence of hot phosphoric acid
Membranes formation
Structure of Polybenzimidazole (PBI) and modified silica
Basic approaches for improving the properties:
incorporation of inorganic particles in PBI matrix capable to stabilize H3PO4
using of surface-modified particles
CONDUCTIVITY
CONCLUSIONS
Hybrid membrane materials based on polybenzimidazole and silica with grafted phosphonic groups for fuel cell applications
The aim of this work is
to study the properties of proton-conducting hybrid membranes based on PBI and silica particles surface-modified by ethylphosphonic-groups.
The grafting of functional –PO3H2 groups onto the silica surface leads to a significant increase in the uptake of phosphoric acid, the concentration of which determines the functional properties of these materials.
The conductivity of the best samples reaches 0.081 S/cm at 160°C.
Due to the contribution of the introduced functional groups to the conductivity, it becomes possible to reduce the amount of introduced acid without a significant loss of conductive properties, which will also contribute to the preservation of mechanical characteristics.
Advantages of PBI
operation temperature 130-180°С
work at low humidity
requirements on fuel purity is reduced (1-3% content of CO), cheap fuel
This work was financially supported by the Russian Science Foundation (project no. 21-73-20229)
Casting PBI polymer solution in N-MP with mixture of tetraethoxysilane and
(2-diethylphosphatoethyl)-
triethoxysilane. Mass fraction of the dopant was 5 or 10%, mole fraction of phosphonic groups was
x = 0–100%).
50% H3PO4 treatment
Drying at 60°C (air) and 120°C (vacuum)
Hydrolysis of
-(OEt)-groups by HCl (18%) treatment with (SiO2)–PO3H2 formation
Fig. 3. Dependence of membrane conductivity on the mole fraction (х) of functional groups for (1, 3) PBI/SiP-5-x and (2, 4) PBI/SiP-10-x at (1, 2) 110°С and (3, 4) 160°С. The data points marked with squares refer to the conductivity of the original PBI-O-PhT membrane at 110 and 160°С.
The introduction of functional groups leads to an increase in the uptake of the acid. For the membranes with a dopant content of 10 wt %, its amount increases by ~10% with an increase in the mole fraction of –PO3H2 groups.
An increase in the concentration of –PO3H2 groups in the dopant facilitates the uptake of a larger amount of acid due to the formation of a system of hydrogen bonds with it.
The incorporation of the unmodified silica into the membrane leads to a slight increase in conductivity.
Along with an increase in the number of functional groups and, accordingly, in the uptake of phosphoric acid, the conductivity of the membranes also increases significantly, reaching 0.081 S/cm at 160°C, which is approximately 2.5 times the conductivity of the reference sample.
The conductivity of these systems is primarily determined by the transport of protons through the system of hydrogen bonds formed by phosphoric acid molecules, the concentration of which in the membrane is much higher. The acidic –PO3H2 groups of the dopant can also contribute to proton transport.
At a high concentration of –PO3H2 groups on the silica surface (10 wt % silica, x > 60), the phosphoric acid content in the membrane becomes too high and the membrane plasticizes at high temperatures.
Fig. 1. TEM-micrograph for PBI/SiO2-5 wt.%-x, x = 0 (a) and x = 100 (b).
Isolated silica particles 3-5 nm in size are uniformly distributed in the membrane.
Increase in phosphonic groups content leads to a little increase in particle size.
a
b
Fig. 2. Dependence of the acid doping level (n H3PO4) on the mole fraction of functional groups (x) in hybrid membranes; the mass concentration of silica is indicated by numbers in the figure.