## Slide 1
Co-axial wet-spun fibers: an innovative strategy for chronic wound healing applications
Catarina S. Miranda1,*, A. F. G. Silva2, S. M. M. A. Pereira-Lima2, S. P. G. Costa2, N. C. Homem3, H. P. Felgueiras1
1Centre for Textile Science and Technology (2C2T)
2Centre of Chemistry (CQ)
3Digital Transformation CoLab (DTx)
University of Minho, Portugal
*catarina.miranda@2c2t.uminho.pt

## Slide 2
Antimicrobial peptides
Alanine-Alanine-Proline-Valine
(Ala-Ala-Pro-Val or AAPV)
Inhibits human neutrophil elastase (HNE), which levels are abnormally high in the case of inflammatory processes related to CWs.
Control microbial proliferation
Modulate immune response
Low MW molecules
Composed of amino acid residues
Antimicrobial Peptides
Low stability in physiological media
Incorporation within polymeric structures
Santos, F.C. et al. Amino Acids, 49 (2017).
2

## Slide 3
Polymers
Sodium alginate (SA)
Antiseptic properties;
Water absorbent (elevated swelling capacity);
Creates a moist environment.
Polycaprolactone (PCL)
Synthetic polymer;
Excellent mechanical properties;
Slow degradation rate.
Plotczyk, M. et al. Elsevier. 1 (2019)
Eskandarinia, A. et al. Scientific Reports. (2020)
Biocompatible; Biodegradable
3

## Slide 4
Polymers
Chemically modified
Chitosan (CS)
N-carboxymethyl chitosan
(NCMC)
Non-toxic;
Soluble at neutral to basic pH’s;
Antimicrobial activity.
Plotczyk, M. et al. Elsevier. 1 (2019)
Song, Q.; Zhang, Z.; Gao, J.; Ding, C. J. Appl. Polym. Sci. 2011, 119, 3282–3285
Strong tissue adhesive properties;
Accelerates tissue repair;
Acts as a hemostatic agent.
Biocompatible; Biodegradable
4

## Slide 5
Wet-spinning
Technique based on a non-solvent-induced phase inversion process, in which a polymeric solution is extruded into a coagulation bath composed of a poor solvent or a non-solvent, giving rise to a continuous polymeric fiber, with a diameter of tens to hundreds of micrometers.
5
Miranda, C. et al. Pharmaceutics, 2022, 14. 164

## Slide 6
Co-axial wet-spinning
Mirabedini, A. (2017). A thesis submitted in the fulfilment of the. 1–235.
Gao, L., Zhou, Y., Peng, J., Xu, C., Xu, Q., Xing, M., & Chang, J. (2019). NPG Asia Materials, 11(1), 66.
McKeen, L. W. (2012). Permeability Properties of Plastics and Elastomers, 59–75.
Co-axial spinneret
Two polymer solutions are injected together into a co-axial spinneret and co-extruded towards a coagulation bath, generating a core-shell structure. In case of hollow fibers, air or coagulation bath is introduced through the innermost port.
Core-sheath fibers
Sheath
Core
Hollow fibers
Sheath
Hollow interior
Sheath solution
Core solution
Co-axial fibers
6

## Slide 7
Goal
Engineer AAPV-loaded microfibers doped with NCMC via wet-spinning for human neutrophil elastase control and Staphylococcus aureus inhibition.
7
In chronic wounds, neutrophil elastase is 10-40% more abundant than in acute wounds.
According to the World Health Organization, S. aureus is one of the most prevalent bacteria in chronic wounds.
Felgueiras, H. et al. Colloids Surf B Biointerfaces 2017
https://www.who.int/

## Slide 8
Co-axial wet-spun fibers
PCL 10% w/v + AAPV IC
0.10 mL/min
SA 2% w/v +
NCMC 2xMBC
0.15 mL/min
Sheath
Core
Side view
Cross-section view
Goal of Each Microfiber Component:
AAPV: regulate HNE enzymatic levels
SA: create and maintain a moist environment
PCL: maintain fibers’ structural integrity
NCMC: antimicrobial activity
8
Produced fibers:
SA hollow (core: coagulation bath; shell: SA);
SA-NCMC hollow (core: coagulation bath; shell: SA combined
with NCMC);
PCL (core: PCL; shell: coagulation bath);
PCL-AAPV (core: PCL combined with AAPV; shell: coagulation
bath);
SA-PCL (core: PCL; shell: SA);
SA-PCL-AAPV (core: PCL combined with AAPV; shell: SA);
SA-NCMC-PCL (core: PCL; shell: SA combined with NCMC);
SA-NCMC-PCL-AAPV (core: PCL combined with AAPV; shell:
SA combined with NCMC)
Coagulation bath: 2% w/v CaCl2
MBC – Minimum Bactericidal Concentration
IC - Concentration providing maximum % of inhibition of HNE activity

## Slide 9
Fibers morphology
9
Macroscopic view
Microscopic view
SEM observation
SEM – Scanning Electron Microscopy

## Slide 10
Inhibition of HNE activity
10
Evaluate AAPV’s action towards HNE’s enzymatic levels
Testing Substrate:
- Tris-HCl-buffer
- N-MeO-Suc-Ala-Ala-Pro-Val-p-NA
AAPV
Spectroscopy readings (405 nm)
HNE
Soybean tripsin inhibitor solution
(to stop the reaction)
Santos, F.C., et al. Amino Acids 2017, 49, 1077–108; Castro, V.I.B., et al. Tetrahedron 2016, 72, 1024–1030.
45 mU/mL, [HNE] in chronic wounds
t = 1 h: initial burst release
SA-NCMC-PCL-AAPV fibers presented the highest HNE inhibition at the 6 h mark.

## Slide 11
Antimicrobial activity
NCMC-loaded fibers inhibited the most bacteria growth.
S. aureus activity was reduced by 90-99% at the 6 h mark.
11
Homem, N.C. et al. Int. J. Mol. Sci. 2021
Testing Parameters:
1 × 105 CFUs/mL S. aureus suspension in Mueller Hinton Broth
Samples of 10 mg immersed in 1 mL of bacteria suspension and incubated at 37 ºC and 120 rpm, for 1, 2, 4, 6 and 24 h;
At each time point, bacteria suspensions were serially diluted in PBS and incubated at 37 ºC for 24 h;
Grown colonies were counted, and results were expressed in log reduction.

## Slide 12
Conclusions
The potential of the engineered co-axial fibers to serve as controlled release platforms for AAPV was demonstrated, along its inhibitory effect against HNE, particularly after 6 h of incubation.
The NCMC antibacterial activity against S. aureus was also established.
Data confirmed the potential of this system to function as a multi-action delivery platform, suitable for prospective wound healing applications.
12

## Slide 13
Acknowledgements
2C2T and CQ Teams
Thank you for your attention.
This work is financed by FEDER funds through COMPETE and by national funds through FCT via the projects POCI-01-0145-FEDER-028074 (PEPTEX) and UID/CTM/00264/2021. C.S.M. acknowledges FCT for the PhD grant with reference 2020.08547.BD.
13