## Slide 1
3rd International Electronic Conference on Applied Sciences
Preparation of alginate hydrogels with carbonated water for wound dressings application
○Ryota Teshima*1, Shigehito Osawa2,3, Miki Yoshikawa4, Hidenori Otsuka1,2,3, Yayoi Kawano*4, Takehisa Hanawa*4
1 Department of Chemistry, Graduate School of Science, Tokyo University of Science, Japan.
2 Department of Applied Chemistry, Faculty of Science, Tokyo University of Science, Japan.
3 Water Frontier Science and Technology Research Center, Research Institute for Science and
Technology, Tokyo University of Science, Japan.
4 Department of Pharmacy, Faculty of Pharmaceutical Sciences, Tokyo University of Science, Japan.
*Corresponding Authors: Ryota Teshima (1322595@ed.tus.ac.jp), Yayoi Kawano, Takehisa Hanawa
1/13

## Slide 2
Introduction
Wound healing with hydrogels
Hydrogel provides moist environment for the wound site
and can promote wound healing.
1. K. Nuutila et al. Adv in Wound Care, 2021. 10. 685-698.
2. Z. Xu et al. Adv. Healthcare Mater. 2020. 9. 1901502.
3. Y. Liang et al. ACS Nano. 2021. 15.12687-127222.
The skin is the largest organ in our body and very vulnerable to external damage.
Depending on the type of the wound site, wound healing can last several years.
Wound healing is promoted by keeping the moist environment of wound site1.
Hydrogel has attracted attention as a wound dressing2,3.
Hydrogels have a three-dimensional polymer network structure that contains numerous water molecules.
2/13
Image citation: https://www.tus.ac.jp/en/mediarelations/archive/20200826_0087.html

## Slide 3
Alginate
Alginate is an anionic polysaccharide extracted from brown algae.
Alginate has high biocompatibility and reacts with Ca2+ to form hydrogels.
The low pH of hydrogel can inhibit cell proliferation
and limit the applicability for wound dressings.
Alginate/CaCO3 solution
Acid Solution
Gelation
“Hydrogel”
CaCO3 + 2H+ → Ca2+ + H2O + CO2
Alginate + Ca2+→ Hydrogel formation
Preparation method of alginate hydrogel5
Residual acidic agent
in the hydrogel
Acidification
of the hydrogel
In these methods…
Alginate hydrogels are widely applied as biomaterials4.
4. C. J. Maxwell et al. J Biomed Mater Res Part A. 2022. 110. 1621-1635.
5. M.C. Straccia et al. Mar. Drugs. 2015. 13. 2890-2908.
3/13
Introduction

## Slide 4
Alginate/ CaCO3
mixed solution
Carbonated water
Gelation
Volatilization of CO2
from hydrogels
Alginate hydrogels
without acidification
CO2 in carbonated water induces gelation by dissolving CaCO3. with temporary pH decrease and volatilizes from the hydrogel6.
→This methods accelerate gelation without acidification of final hydrogel.
In this study, the physicochemical properties and wound-healing effects of hydrogels were evaluated.
In vivo wound healing
Hydrogels
4/13
6. R. Teshima et al. Polym Adv Technol. 2020. 31. 3032-3038.
Purpose of this study

## Slide 5
2.0 (w/v%) Alginate /
0.15-0.30(w/v%) CaCO3
mixed solution 20 mL
Gelation
Carbonated water 10 mL
(pH=3.81±0.08, n=19)
The mixed solution transited to a hydrogel within 4 min.
Gelation time
Hydrogel preparation
Prepared hydrogel
Gel volume: 5 mL, Temperature: 23-25℃, Values are expressed as the mean±SD; n=3 (Error bars were smaller than the plot size).
The prepared gel was transparent
and could be handled with tweezers.
Tip width = 6 mm
The gelation time can be controlled with CaCO3 concentration.
5/13
Results and Discussion

## Slide 6
Water absorption test
Water contents
Hydrogel disk
×1 PBS
30 mL
24 h
immersion
Hydrogel disk: φ17.5 mm×3.5 mm, Temperature: 23-25℃, Values are expressed as the mean±SD;n=3.
CaCO3 conc.(w/v%) | Water content(%)
0.15 | 98.6±0.2
0.20 | 98.7±0.1
0.30 | 98.5±0.1
Hydrogel disk: φ17.5 mm×3.5 mm, Values are expressed as the mean±SD; n=3.
All hydrogels had high water content (~99%).
All hydrogels absorbed ×1 PBS solution.
Wp= the weight of prepared gel, Ws= the weight of the swollen gel
Ww= the weight of prepared gel, Wd= the weight of dry gel.
The hydrogel provides an adequate moist environment
to the wound site and can maintain exudate.
6/13
Results and Discussion

## Slide 7
Surfaces pH measurements of hydrogels
Hydrogel disk: φ17.5 mm×3.5 mm, CaCO3 concentration: 0.20 (w/v%), Temperature: 23-25℃, Values are expressed as the mean±SD; n=3-6.
Thickness = 1.23±0.38 mm
Thickness = 3.46±0.32 mm
Thickness = 5.89±0.29 mm
Gel thickness= 1.23±0.38 mm, 3.46±0.32 mm, 5.89±0.29 mm
The surfaces pH was measured
by flat electrode over time.
CO2 volatilizes through the front surface of hydrogels and
final pH is suitable for fibroblast and epidermal cell growth.
Convergent pH =~8.5
Convergent pH =~8.5
No convergence
7/13
Results and Discussion

## Slide 8
Hydrogel disk: φ17.5 mm×3.5 mm, New Coccine (NC) concentration in gels: 1.98 mg/g-gel, Temperature: 23-25℃, Physiological saline volume: 100 mL, Stirring speed: 200 rpm, Values are expressed as the mean±SD; n=2.
Release behavior of New Coccine from hydrogel
New Coccine (NC)
The hydrogel with NC
(1.98 mg/g-gel)
Physiological saline
100 mL
Release devise
The hydrogel released ~90% of NC from hydrogel surface within 300 min.
The hydrogels have potential application for
drug delivery material on wound site.
Molecular Weight = 604.5
8/13
Alg-Cax : x = CaCO3 concentration
Results and Discussion

## Slide 9
Chart: Cell viability (%)
| 0.15(w/v) % CaCO3 gels | 0.20(w/v) % CaCO3 gels | 0.30(w/v)% CaCO3 gel | Control
 | 102.0889 | 100.5957 | 100.254 | 100
Alg-Ca0.15
Alg-Ca0.20
Alg-Ca0.30
Control
Hydrogel disk
(immersed in DMEM)
DMEM 1 mL
(10% FBS, 2% PS)
NHDF
DMEM 360 μL
Control
DMEM 1 mL
(10% FBS, 2% PS)
NHDF
Hydrogel disk: φ11.5 mm×3.5 mm, CaCO3 concentration: 0.20 (w/v%), Cell: Normal Human Dermal Fibroblasts (NHDF), Passage: p15 ,Cell density: 2.5×104 cells/well, pre-Incubation time: 12 h (37℃, 5% CO2), Incubation time: 24 h (37℃, 5% CO2), Values are expressed as the mean±SD ;n=4.
Biocompatibility of hydrogels
24 h culture
The hydrogels have biocompatibility.
CCK-8 Assay
Hydrogels prepared in this study do not inhibit NHDF cells proliferation.
9/13
Alg-Cax : x = CaCO3 concentration
Results and Discussion

## Slide 10
NHDF
DMEM 1 mL
Hydrogel disk
(250 μL)
NHDF
DMEM 1 mL
Gel volume: 250 μL, CaCO3 concentration: 0.20 (w/v%), Cell: Normal Human Dermal Fibroblasts (NHDF) Passage: p11 ,Cell density: 2.0×104 cells/well, Incubation time: 17 h (37℃, 5% CO2)
Cell adhesion test of hydrogels
Hydrogel can be exchanged without damaging tissue.
Cells were cultured
on TC plate.
Cells were cultured
on gel surface.
Control
NHDF formed aggregation structures (“Spheroids”) on the gel surface.
→ NHDF do not adhere to hydrogel surface.
Spheroids
10/13
Results and Discussion

## Slide 11
Experimental model with full-thickness skin defects
Wound site
Dressings
(Gauze and hydrogels)
TegadermTM (3M)
(Secondary dressing)
Excisional wound formation
Attachment of dressings
Wound Dressings
Dry Gauze (Libatape, Japan)
VIEW GEL®︎(clinical hydrogel dressings, Nichiban, Japan)
Alginate hydrogels prepared in this study
(Gel thickness = ~1.2 mm, CaCO3 concentration = 0.20 w/v%)
Wound average area = 29.8 mm2
Weight average = 34.6 g
This animal experiment was approved by
Ethical Committee of Tokyo University of Science, Japan (Protocol Y21024).
C57BLKS/JIar- +Leprdb/ +Leprdb mice
11/13
Results and Discussion

## Slide 12
Chart: Time (day)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14
Gauze | 100 | 96.5482 | 92.9111 | 88.0576 | 87.1817 | 71.6101 | 75.1139 | 72.5919 | 63.4889 | 68.9102 | 56.8503 | 54.8809 | 51.4584 | 42.121 | 45.2669
VIEW GEL | 100 | 134.4814 | 114.6214 | 114.1512 | 106.4908 | 70.2044 | 56.0312 | 45.5501 | 30.3691 | 26.4501 | 13.8429 | 10.7724 | 8.2664 | 9.4178 | 10.0153
Alginate gels | 100 | 113.5975 | 110.9945 | 100.9807 | 90.7329 | 71.3391 | 62.7269 | 53.9207 | 45.2498 | 39.4335 | 24.1543 | 17.0507 | 4.7956 | 4.9404 | 6.2876
Change of wound area
The hydrogel prepared in this study showed excellent wound healing effects.
Chart: Wound area (%)
| Gauze | VIEW GEL | Alg-Ca2.0
 | 45.2669 | 10.0153 | 6.2876
Gauze
VIEW GEL®︎
Alginate gels
*
45.3%
10.0%
6.3%
Values are expressed as the mean±SE ;n=4. *p<0.05
Alginate hydrogel promoted wound healing compared to dry gauze.
12/13
Results and Discussion

## Slide 13
Conclusions
Kimica Corporation (Tokyo, Japan) for supplying alginate in this study.
Prof. Akihiko Kikuchi, Tokyo University of Science, for valuable discussions.
This work was supported by Masason Foundation and Kouyoukai (Tokyo University of Science).
Acknowledgment
This study thoroughly evaluated the property of alginate hydrogel
with carbonated water and its wound healing effects.
Hydrogels
The addition of carbonated water induced gelation of alginate hydrogel in short time.
The prepared hydrogels have high water content (~99%).
The surfaces pH of hydrogels are suitable for skin cell growth.
The hydrogels have biocompatibility and can be exchanged without damaging tissue.
The hydrogels prepared in this study showed excellent wound healing effects.
13/13