## Slide 1
Additive effects of lanthanide compound into CH3NH3PbI3 perovskite layer on the photovoltaic properties and electronic structure
*A. Suzuki1, K. Kishimoto1, T. Oku1,
M. Okita2, S. Fukunishi2, T. Tachikawa2, and T. Hasegawa2
1 The University of Shiga Prefecture, Shiga 522-8533, Japan
2 Osaka Gas Chemicals Co., Ltd., Osaka 554-0051, Japan
ASEC 2022 The 3rd International Electronic Conference on Applied Sciences 01-15 Dec. 2022

## Slide 2
Wang et al., Science 363 (2019) 265–270.
A. Suzuki, T. Oku, Jpn. J. Appl. Phys. 57 (2018) 02CE04-1-7.
A. Suzuki, M. Oe, T. Oku, J. Electron. Mater. 50 (2021) 1980.
A. Suzuki, T. Oku, Heliyon 4 (2018) e00755-1-22, A. Suzuki, T. Oku, Mater. Adv. 2 (2021) 2609-2616.
Perovskite solar cell
Elements, Crystal structure
Voc > 1.0 V Si, Eg ≈ 1.6 eV,
η ≈ Si, GaAs]
Conversion region (300 - 800 nm)
Simple process by spin coating
Easy to decompose,
Challenges for stability
Lanthanoid compounds: Eu (II), Sm (III), Tb (III)
⇒ Stability of the photovoltaic performance
Energy diagram of solar cell
Perovskite solar cell
Perovskite crystal
CH
3
NH
3
+
(MA
+
)
Pb
2
+
I
-
Introduction

## Slide 3
lanthanide (Ln) compound
4f-spin in Ln is less susceptible to the effect of crystal field
Eu3+: 4f-4f transition Red fluorescence
⇒Up/down conversion materials for solar cell
Eu2+: 4f65d1 transition wide fluorescence
Magnetism, high spin state (4f7 J = S = 7/2) (I = 5/2)
M. Pazoki, et. al. J. Mater. Chem. A, 5 (2017) 23131
b)
Charge density of MAEuI3 perovskite calculated by DFT+U
Localization
Wang et al., Science 363, 265–270 (2019)
Purpose: Electronic structures of lanthanide (Eu, Sm, Tb, Ce) incorporated perovskite crystal were calculated by first-principles calculation, and characterization of lanthanide compound incorporated CH(NH2)2PbI3 (FAPbI3) perovskite solar cell was performed for improving the photovoltaic performance.
Incorporation of Eu suppressed the decomposition
⇒ Long-term of stability, Improved performance
Notes: 最近、希土類元素であるEuを導入したペロブスカイト太陽電池が作製され、その性能が報告されています。Euの酸化還元機構を利用してペロブスカイト層の分解が抑制され、長期安定性や性能向上が報告されています。
本研究の目的は、希土類元素である(Eu, Sm, Tb, Ce)を部分置換したペロブスカイト結晶の電子構造を第一原理計算により予測し、光起電力特性である短絡電流密度や変換効率の向上を検証することである。
Rare-earth-based compound with heavy-electron behavior have unique type of physical phenomena such as magnetic properties, fluorescence characteristics and superconductivity.
For example, the 4f electrons of europium are blocked by the closed shell structure of 5s-5p6.
The europium compound (EuIII) emits a sharp red fluorescence based on 4f-4f transition,
applying wavelength converter for solar cells.
The europium compound (EuII) had a wide area of fluorescence, electron correlation between d orbital and conductive carrier based on metal-ligand charge transfer in the coordination structure.
The heavy-electron behavior based on localized 4f orbital will be considered by the electronic structure and effective mass.

## Slide 4
First-principle calculation

## Slide 5
(a) Electronic density distribution, (b) band structure and (c) partial density of state (PDOS) of Tb(III)-doped FAPbI3 perovskite crystals
PBE, k = 4 x 4 x 4, Cubic, a = 12.72 Å
(b)
(c)
Tb: 4f9 5d 6s2
Eg = 1.49 eV
Total energy -4725 eV cell-1
ΔE = -980 eV cell-1
0.05
-0.01
(a)
FA FA
I Tb I
I Pb I
I
Electron density distribution
Band structure
Partial density of state (PDOS)
Electronic structure of FAPbTb(III)I3
Notes: FAPbTb(III)I3ペロブスカイト結晶の電子密度分布、バンド構造、部分状態密度を示します。
Tb, I原子の電子密度分布は高く、Tb – I結合間の相互作用は弱い。
価電子帯では局在化したTb 4f軌道が出現し、配位子I p軌道との相互作用は弱く、電荷移動は抑制され、
ホール移動、Jsc, ηは低下すると予想される。
伝導帯ではPb p軌道から離れたところにTb d軌道が出現し、電荷移動の影響は少ない。
バンドギャップは1.49 eVとなり、開放電圧はFAPbI3系と同様の結果が予想される。
全エネルギーはFAPbI3系よりも低下し、Tb(III)添加によりエネルギー的に安定性を示す。

## Slide 6
Total energies of the doped-FAPbI3 cluster and crystals.
Doped-cluster Total energy (eV cell-1) Δ E a (eV cell-1)
FAPbI3 -6513 0
Eu2+ -8918 -2405
Eu3+ -8915 -2402
Sm2+ -5417 1096
Tb3+ -5894 619
Eu2+, Cl- -11971 -5458
Eu2+, Br- -8931 -2418
Doped-crystal Total energy (eV cell-1) Δ E a (eV cell-1)
FAPbI3 -3745 0
Eu2+ -4582 -837
Eu3+ -3714 31
Sm2+ -3538 207
Tb3+ -4725 -980
Ce4+ -3500 245
a △ E: difference between the total energy of the doped-FAPbI3 and FAPbI3 clusters and crystals
Stability
Stability
Stability
Notes: Lanthanide—doped perovskite結晶の全エネルギーを表に示す。
Euを導入した系の全エネルギーは低下し、安定性を示した。
Total energies of Eu-doped cluster and crystals were decreased as compared with other cases,
yielding thermal stabilities of conversion efficiency.
Gd-doped crystal total energy

## Slide 7
Chart: Voltage (V)
| 0.93351999999999991 | 0.90620000000000001 | 0.87891399999999997 | 0.85155899999999995 | 0.82423899999999994 | 0.79691999999999996 | 0.76959999999999995 | 0.74227899999999991 | 0.71495999999999993 | 0.687639 | 0.66032000000000002 | 0.63300000000000001 | 0.60567899999999997 | 0.57835899999999996 | 0.55103999999999997 | 0.52371999999999996 | 0.49639999999999995 | 0.46908 | 0.44175899999999996 | 0.41443999999999998 | 0.38711899999999999 | 0.35979899999999998 | 0.33248 | 0.30515999999999999 | 0.27783999999999998 | 0.25051899999999999 | 0.22319899999999998 | 0.19587979999999999 | 0.16856019999999999 | 0.1412399 | 0.11391989999999999 | 8.6600299999999991E-2 | 5.9279599999999995E-2 | 3.1960200000000001E-2 | 4.6397999999999995E-3 | -2.26798E-2 | -5.00004E-2
 | -3.3879 | -1.1502 | 0.70056 | 2.1989 | 3.3798 | 4.3222 | 5.0873 | 5.736 | 6.2975 | 6.7869 | 7.249 | 7.649 | 8.0043 | 8.378 | 8.6676 | 8.9444 | 9.1903 | 9.4018 | 9.5954 | 9.7014 | 9.8551 | 9.96 | 10.0424 | 10.1239 | 10.2072 | 10.2816 | 10.3072 | 10.3433 | 10.3756 | 10.4315 | 10.4947 | 10.524 | 10.5927 | 10.6337 | 10.6823 | 10.7305 | 10.8197
 | -6.8125 | -2.9459 | 0.43386 | 3.3465 | 5.7371 | 7.6584 | 9.184 | 10.3392 | 11.2227 | 11.9109 | 12.428 | 12.8232 | 13.1715 | 13.4406 | 13.6291 | 13.8135 | 13.9367 | 14.044 | 14.1239 | 14.2051 | 14.2275 | 14.3356 | 14.3459 | 14.4151 | 14.4006 | 14.4688 | 14.4744 | 14.4764 | 14.4906 | 14.5311 | 14.5459 | 14.5162 | 14.5202 | 14.54 | 14.549 | 14.5535 | 14.5691
 | -3.3957 | -0.70353 | 1.2716 | 2.7521 | 3.8621 | 4.7187 | 5.4023 | 5.9619 | 6.4395 | 6.8358 | 7.1833 | 7.4756 | 7.7403 | 7.9495 | 8.1344 | 8.3199 | 8.4645 | 8.6182 | 8.7084 | 8.8171 | 8.9055 | 8.9811 | 9.0594 | 9.0844 | 9.149 | 9.1558 | 9.2428 | 9.2614 | 9.2971 | 9.3057 | 9.3152 | 9.3395 | 9.3612 | 9.3962 | 9.3946 | 9.4075 | 9.4063
 | -2.9679 | -0.55152 | 1.3389 | 2.8014 | 3.9298 | 4.8029 | 5.5043 | 6.0545 | 6.4983 | 6.8689 | 7.1958 | 7.443 | 7.6849 | 7.887 | 8.0566 | 8.2038 | 8.2937 | 8.4318 | 8.4951 | 8.5966 | 8.6631 | 8.7041 | 8.7339 | 8.7723 | 8.7944 | 8.807 | 8.8448 | 8.8508 | 8.8747 | 8.8876 | 8.8808 | 8.9064 | 8.8962 | 8.8879 | 8.9022 | 8.9105 | 8.9353
 | -4.7308 | -0.43872 | 3.156 | 6.1601 | 8.5922 | 10.5834 | 12.165 | 13.4216 | 14.4099 | 15.1631 | 15.8056 | 16.2689 | 16.6608 | 16.9111 | 17.1306 | 17.3858 | 17.5411 | 17.65 | 17.7613 | 17.7881 | 17.8165 | 17.8673 | 17.8385 | 17.8326 | 17.8414 | 17.868 | 17.7964 | 17.7895 | 17.7324 | 17.674 | 17.6529 | 17.6276 | 17.5886 | 17.5665 | 17.5617 | 17.4898 | 17.5084
J-V characteristics of the solar cells
Perovskite 190 ℃ | Jsc (mA cm-2) | Voc (V) | FF | Rs (Ω cm2) | Rsh (Ω cm2) | η (%) | ηave (%)
FAI 20% | 14.5 | 0.874 | 0.640 | 7.46 | 3950 | 8.13 | 7.40
FAI 10%+EuCl2 2% | 17.6 | 0.860 | 0.659 | 6.57 | 3960 | 9.94 | 8.30
FAI 10%+EuBr2 1% | 10.7 | 0.889 | 0.510 | 14.6 | 622 | 4.85 | 4.66
FAI 10%+EuBr2 2% | 9.40 | 0.883 | 0.563 | 11.5 | 1690 | 4.67 | 3.59
FAI 20%+EuBr2 2% | 8.90 | 0.875 | 0.594 | 12.3 | 4760 | 4.62 | 4.34
Photovoltaic parameters of the perovskite solar cells with FAI and Eu.
FAI 20%
FAI 10%
+EuCl2 2%
FAI 10%
+EuBr2 1%
FAI 10%
+EuBr2 2%
FAI 20%
+EuBr2 2%
Stabilities of conversion efficiency
(a)
FAI 10%,
EuCl2 2%
30 days
stability
Chart: 
| 0 | 30 | 180 | 260 | 320
 | 8.5883 | 7.9683 | 3.1439 | 3.9368 | 2.5296
最大 | 9.9409 | 10.2759 | 3.8844 | 4.1588 | 3.2986
最小 | 7.52 | 5.584 | 2.3937 | 3.7148 | 1.9034
EuCl平均 | 7.4553 | 5.959 | 5.193
EuCl最大 | 8.1287 | 6.0881 | 5.3792
EuCl最小 | 6.8362 | 5.6988 | 4.9752
EuBr1平均 | 4.6156 | 4.0019 | 3.1936
EuBr1最大 | 4.8482 | 4.1961 | 3.7055
EuBr1最小 | 4.3424 | 3.7719 | 2.7433
EuBr2平均 | 3.4312 | 2.8892 | 1.2517
EuBr2最大 | 4.6745 | 3.1484 | 1.6553
EuBr2最小 | 2.0322 | 2.5958 | 0.92521
(b)
Results and Discussion
Notes: Euを導入した系の電流-電圧特性と変換効率の経時変化を示す。
FAI 10%, EuCl2 2%導入によって短絡電流密度、極性因子、並列抵抗が改善し、変換効率が向上した。
変換効率は30日間維持し、安定性を示した。
Figures show J-V characteristics and stability of conversion efficiency for the perovskite solar cells.
The photovoltaic parameters of the perovskite solar cell are listed in Table.
Addition of 10% FAI and 2% EuCl2 improved the photovoltaic parameters such as shirt circuit current density and fill factor related to η.
Addition of FAI and EuCl2 maintained the stability of η for 30 days.

## Slide 8
Chart: 
| 0 | 7
 | 1.2257 | 0.17213
Sm190最大 | 1.3385 | 0.33861
Sm190最小 | 1.1349 | 0.038125
Sm210 | 4.4294 | 0.099868
Sm210最大 | 4.6633 | 0.23172
Sm210最小 | 4.1547 | 0.004764
Tb190 | 5.1696 | 0.77202
Tb190最大 | 5.1916 | 0.8909
Tb190最小 | 5.146 | 0.64246
Tb210 | 7.1086 | 0.3874
Tb210最大 | 7.9288 | 0.43907
Tb210最小 | 6.1632 | 0.32559
Chart: Voltage (V)
| 0.9356819999999999 | 0.9083 | 0.88091999999999993 | 0.85353899999999994 | 0.82615899999999998 | 0.79877900000000002 | 0.77139999999999997 | 0.74401799999999996 | 0.71663299999999996 | 0.68925700000000001 | 0.66188099999999994 | 0.63450299999999993 | 0.60711999999999999 | 0.579739 | 0.55235999999999996 | 0.52498 | 0.49759999999999999 | 0.47021999999999997 | 0.44283999999999996 | 0.41545899999999997 | 0.38807999999999998 | 0.36069999999999997 | 0.33332099999999998 | 0.30593999999999999 | 0.278559 | 0.25117899999999999 | 0.2238 | 0.19642039999999999 | 0.16904039999999998 | 0.14166049999999999 | 0.11427949999999999 | 8.6899299999999999E-2 | 5.9519799999999998E-2 | 3.2139099999999997E-2 | 4.7600999999999997E-3 | -2.2620499999999998E-2 | -5.00004E-2
 | -0.19865 | -0.09185 | 0.017714 | 0.12924 | 0.2434 | 0.36006 | 0.48561 | 0.61632 | 0.75683 | 0.91272 | 1.0818 | 1.2442 | 1.424 | 1.6094 | 1.8258 | 2.0296 | 2.2822 | 2.5171 | 2.7914 | 3.0598 | 3.3682 | 3.6649 | 4.0131 | 4.3586 | 4.67 | 5.007 | 5.3929 | 5.7561 | 6.0243 | 6.3352 | 6.638 | 6.902 | 7.1859 | 7.5137 | 7.7222 | 7.9524 | 8.1313
 | -4.581 | -2.1398 | 0.006219 | 1.8638 | 3.4191 | 4.6958 | 5.6911 | 6.4904 | 7.101 | 7.569 | 7.9435 | 8.2331 | 8.4452 | 8.662 | 8.8702 | 9.0329 | 9.162 | 9.2763 | 9.3818 | 9.4539 | 9.5563 | 9.6696 | 9.708 | 9.8018 | 9.8939 | 9.956 | 10.031 | 10.0762 | 10.1687 | 10.207 | 10.2769 | 10.3482 | 10.4087 | 10.4852 | 10.5718 | 10.6602 | 10.7205
 | -1.984 | -0.7278 | 0.47326 | 1.6073 | 2.6709 | 3.638 | 4.5227 | 5.2908 | 5.964 | 6.5311 | 6.9973 | 7.3895 | 7.7078 | 7.9871 | 8.2491 | 8.4663 | 8.635 | 8.7888 | 8.9169 | 9.0288 | 9.1233 | 9.2302 | 9.3179 | 9.3879 | 9.4603 | 9.5297 | 9.5895 | 9.6583 | 9.6978 | 9.7696 | 9.8264 | 9.8425 | 9.9216 | 9.9383 | 9.9925 | 10.0199 | 10.0845
 | -5.066 | -2.0843 | 0.53932 | 2.8472 | 4.811 | 6.4659 | 7.8582 | 8.9879 | 9.9204 | 10.6916 | 11.3404 | 11.8766 | 12.3114 | 12.709 | 13.0147 | 13.3126 | 13.5241 | 13.7359 | 13.888 | 14.0203 | 14.1096 | 14.1954 | 14.2334 | 14.291 | 14.3675 | 14.3989 | 14.4543 | 14.4642 | 14.5033 | 14.5468 | 14.5548 | 14.5806 | 14.5475 | 14.5797 | 14.6087 | 14.6325 | 14.6442
 | Jsc (mA cm-2) | Voc (V) | FF | Rs (Ω cm2) | Rsh (Ω cm2) | η (%) | ηave (%)
190℃ Sm | 7.76 | 0.885 | 0.195 | 100 | 118 | 1.34 | 1.20
210℃ Sm | 11.2 | 0.891 | 0.440 | 23.6 | 455 | 4.79 | 4.54
190℃ Tb | 10.6 | 0.870 | 0.564 | 11.8 | 421 | 5.19 | 5.17
210℃ Tb | 14.6 | 0.932 | 0.582 | 10.9 | 2030 | 7.93 | 7.23
Sm 190℃
Tb 210℃
Tb 190℃
Sm 210℃
J-V characteristics of the solar cells.
Photovoltaic properties of perovskite solar cells
Stabilities of conversion efficiency
FAI 20%
Sm, Tb 2%
(a)
(b)
JV curve
Stability of η
decomposition
Notes: Sm, Tbを導入した系の電流-電圧特性と変換効率の経時変化を示す。
Sm, Tb導入系は熱処理温度210℃で短絡電流密度、極性因子、並列抵抗が改善し、変換効率が向上した。
しかし、変換効率は7日間で低下し、安定性を示さなかった。
J-V characteristics and stability of conversion efficiency for the added with Sm- and Tb-doped perovskite solar cells
are shown in Figures and table.
Incorporation of Tb into the perovskite layer improved the photovoltaic parameters of shirt circuit current density,
open circuit voltage, FF, series resistance, shunt resistance related to η. Stabilities of η were reduced for 1 week.

## Slide 9
Chart: Wavelength (nm)
 | 0 | 13.1 | 19.98 | 22.27 | 22.3 | 21.02 | 19.82 | 19.61 | 22.84 | 23.18 | 23.77 | 24.11 | 26.43 | 29.08 | 31.2 | 32.96 | 34.08 | 35.61 | 35.12 | 33.86 | 34.52 | 34.48 | 34.52 | 34.42 | 34.16 | 33.69 | 33.03 | 32.19 | 31.42 | 30.82 | 29.98 | 29.25 | 28.56 | 28.02 | 27.02 | 26.2 | 25.25 | 24.39 | 24.38 | 24.58 | 24.15 | 23.5 | 23.54 | 22.74 | 21.52 | 17.75 | 12.39 | 7.05 | 0 | 0 | 0
 | 0 | 11.18 | 16.48 | 18.5 | 18.84 | 18.1 | 17.28 | 17.37 | 19.7 | 20.19 | 20.88 | 21.26 | 23.59 | 26.64 | 29.16 | 31.25 | 32.68 | 34.24 | 34.27 | 34.1 | 35.38 | 35.85 | 36.36 | 36.73 | 36.93 | 36.94 | 36.81 | 36.34 | 35.93 | 35.64 | 35.23 | 34.85 | 34.43 | 34 | 33.32 | 32.5 | 31.82 | 30.96 | 31.14 | 31.57 | 31.4 | 30.83 | 31.02 | 29.93 | 29.38 | 25.82 | 19.33 | 11.36 | 3.33 | 0 | 0
Chart: Wavelength (nm)
FAI 20%
FAI 10%+EuCl2 2%
FAI 10%
+EuBr2 1%
FAI 10%
+EuBr2 2%
FAI 20%
+EuBr2 2%
EQE of the perovskite solar cells with (a) Eu, FA and (b) Sm or Tb.
FAI 10%, EuCl2 2% EQE Up, Tb, Sm 190℃→210℃ EQE increased
190℃ Sm
210℃ Tb
190℃ Tb
210℃ Sm
(a)
(b)
FAI 20%
External quantum efficiency (EQE)

## Slide 10
Electronic structure of lanthanide incorporate perovskite crystal was expected by first-principles calculation. The experimental investigation was performed.
Incorporation of Eu promoted the charge transfer, increasing Jsc related to η. Localization of d, f orbital of Sm, Tb, Ce near VB and CB suppressed the carrier diffusion, decreasing Jsc related to η.
Conclusion
The calculation prediction could be proved from the experiments.