## Slide 1
Introduction
Materials and methods
Metamaterials are artificially designed materials with properties that derives from their sub-wavelength structure. Optical metamaterials enable strong light-matter interaction over a broad range of the electromagnetic spectrum not achievable by any existing material in nature. Using MPL for metamaterial research is further underlined by demonstrating a procedure to process metamaterials operating at low THz.
As a photosensitive material for the MPL an organic – inorganic photopolymer SZ2080™[1] was used. The structures were further processed using selective electroless plating to cover the polymer with silver via chemical procedure[2] in order to create a metallo-dielectric material. Simulations were done first with FDTD to define the optimal geometry and experimental measurements of S-parameters conducted after MPL process.
3D THz metamaterial filter for low THz
Fig 2. SEM image of fabricated metamaterial.
Fig 3. Results for TE mode
Fig 4. Results of TM mode.
Fabrication and analysis of 3D low THz metamaterials
S. Papamakarios1,2 *, O. Tsilipakos2,3, A. Koulouklidis2, S. Tzortzakis2,3, M. Kafesaki2,3, M. Farsari2 *
Department of Physics, University of Crete, Vassilika Vouton, Heraklion, 71409, Greece
Institute of Electronic Structure and Laser, Foundation for Research and Technology – Hellas (FORTH – IESL) , 100 Nikolaou Plastira Street, Heraklio, 70013, Greece
Department of Materials Science and Technology, University of Crete, Vassilika Vouton, Heraklion, 71409, Greece
* spapamakarios@physics.uoc.gr
References
Farsari, M., Chichkov, B. Two-photon fabrication. Nature Photon 3, 450–452 (2009). https://doi.org/10.1038/nphoton.2009.131
Sakellari, I., Yin, X., Nesterov, M. L., Terzaki, K., Xomalis, A., Farsari, M., Advanced Optical Materials 2017, 5, 1700200. https://doi.org/10.1002/adom.201700200
Funding
This research project has received funding from the EU's H2020 framework programme for research and innovation under grant agreement NFFA-Europe-Pilot (n. 101007417)
State of the art metamaterial design
y TE(0,0)
x TM(0,0)
x TM(0,0)
  Selective electroless silver coating
Fig 2. SEM image of silver coating.
Table 1. EDX measurement on the fabricated structure.
Table 2. EDX measurement on the substrate.
  SEM images
Fig 1. Images of the fabricated structure.
Fig 1. Image of metallic metamaterial.
y TE(0,0)
Asymmetric U-SRR
Symmetric U-SRR
Electromagnetically Induced Transparency (EIT)
k