## Slide 1
Synthesis of carboxylated magnetite nanoparticles
covalent conjugates with folic acid antibody FA-1 for
lateral flow immunoassay
Moscow
2023
Zolotova M.O., Znoyko S.L.,
Orlov A.V., Nikitin P.I., Sinolits A.V.
2nd International Electronic Conference on Chemical Sensors and Analytical Chemistry

## Slide 2
Objectives and tasks
To obtain magnetite nanoparticles able to conjugate with
folic acid antibodies covalently
Objective
Tasks
Preparation of magnetite nanoparticles
Functionalization of magnetite nanoparticles with amino- and carboxyl groups
Conjugation of carboxylated magnetite nanoparticles with folic acid antibodies FA-1
Testing and quantifying of bonding of magnetite nanoparticles conjugates with antibodies with folic acid with magnetometric assay

## Slide 3
Synthesis of MNPs
4

## Slide 4
TEOS, H2O, Et3N
APTES, EtOH
Functionalization of magnetic nanoparticles
2 hour
tetraethoxysilane (TEOS)
30 min
APTES
succinic anhydride
DMFA, Et3N
succinic anhydride
2 hour

## Slide 5
Results and discussion
Hydrodynamic radii of particles in MNP suspensions
XRD of MNPs synthesized
6
ζ-potential | 
MNP | 0 mV
MNP-cit | -48±7 mV
MNP-NH2 | +25±7 mV
MNP-COOH | -25±10 mV

## Slide 6
lgG
folic acid antibody
Magnitometry
FA-gelatin
Fe3O4-lgG
Fe3O4-lgG-FA-gelatin
EDC
Magnetic particle quantification (MPQ) technique

## Slide 7
Test stripes:
MNP-COOH
Control
Magnetograms of test stripes with MNP-COOH-EDC-FA-1 against FA-gelatin conjugates
Magnetic particle quantification (MPQ) technique

## Slide 8
Synthesis of MNPs in Ar atmosphere allows obtaining MNPs without any other phases but magnetite
MNPs may serve both as a platform for immobilization of antibodies and a magnetic label for them
MPQ may be quite a precise tool for detection and quantitative analysis of MNPs, so the magnetometric lateral flow immunoassay is possible with use of them, for example, to quantify the interaction antibody-antigen
Conclusions