## Slide 1: Bimodal nanoprobes containing AgInSe2 hydrophilic quantum dots and paramagnetic chelates for diagnostic magnetic resonance imaging
*rebeca.muniz@ufpe.br
1Department of Fundamental Chemistry, Federal University of Pernambuco, Recife, Brazil
2Department of Chemistry & CESAM, University of Aveiro, Portugal
Rebeca Muniz de Melo1,*, Gabriela M. Albuquerque1, Goreti Pereira1,2, Giovannia A. L. Pereira1

## Slide 2: Introduction
Magnetic Resonance Imaging (MRI)
No contrast agent
With contrast agent
2

## Slide 3: Introduction
Nanoparticulate Contrast Agents (CAs):
Quantum Dots - QDs
QD
Bimodal Nanoprobes
CAs more efficient
With high relaxivities;
Increased technique sensitivity.
3

## Slide 4: Objectives
Prepare cadmium-free QDs (AgInSe2) and conjugate them with Gd3+ complexes, for the preparation of bimodal probes that combine paramagnetic and optical properties for diagnostic imaging.
4

## Slide 5: Methodology
Preparation of AgInSe2 QDs (AISe)
AgNO3 + In(NO3)3 + MSA
NaBH4
e
Na2SeO3
Miscellaneous parameters:
Temperature;
Molar ratio of Ag:In;
Quantity of MSA;
Quantity of Se;
Reaction time.
15 syntheses
5
The QDs were characterized by UV-Vis absorption (Evolution 600 spectrophotometer, Thermo Scientific) and emission (LS 55 spectrometer, PerkinElmer) spectroscopy.

## Slide 6: Methodology
Preparation of the complex Gd3+ : DOTA-Gd-CYA
Gd3+
(GdCl3)
DOTA
EDC
NHS
cysteamine (CYA)
DOTA-CYA
6
The complex was characterized by relaxometry (Minispec Bruker 20 MHz) and the xylenol orange test using a UV-Vis absorption spectrophotometer.

## Slide 7: Methodology
Preparation of the Bimodal System (AISe-DOTA)
Quantum Dot
DOTA-CYA
AgInSe2
AgInSe2
Bimodal System
(AISe-DOTA)
7
The bimodal systems were characterized by UV-Vis absorption and emission spectroscopy and by relaxometry.

## Slide 8: Results
Preparation of AgInSe2 QDs (AISe)
Absorption spectra of AISe QDs syntheses.
Emission spectra of AISe QDs syntheses.
8

## Slide 9: Results
Preparation of the complex Gd3+ : DOTA-Gd-CYA
Complexation yield of the Gd3+ complexes prepared with the DOTA linker, without and with the linker, and relaxivity of the prepared complexes (20 MHz and 37 ºC).
CAs used clinically (DOTA-Gd = 3.4 mM-1s-1, at 20 MHz and 37 ºC, in water).
9
Sample | Complexation yield (%) | r1 (mM-1s-1)
DOTA-Gd | 98,8 | 3,83
DOTA-Gd-CYA | 98,7 | 3,75

## Slide 10: Results
Preparation of the Bimodal System (AISe-DOTA)
Absorption and emission spectra of the bimodal system QD+DOTA-CYA (AISe-DOTA) and QD.
Found values of longitudinal relaxivity r1 of bimodal systems (20 MHz em 25 °C and 37 ºC).
10
Sample | V (m) | r1 (mM-1s-1) 25 °C | r1 (mM-1s-1) 37 °C
AISe-DOTA 1 | 50 | 5,20 | 5,23
AISe-DOTA 2 | 100 | 6,78 | 6,30
Sample |  | r1 (mM-1s-1) 25 °C | r1 (mM-1s-1) 37 °C
AISe-DOTA 1 | 50 | 5,20 | 5,23
AISe-DOTA 2 | 100 | 6,78 | 6,30
(DOTA-Gd = 3,4 mM-1s-1, à 20 MHz and 37 ºC, in water)
*per Gd3+, considering the total DOTA-Gd added.

## Slide 11: Conclusion
The heating methodology used to prepare the complexes proved to be effective;
With a promising and easy-to-execute conjugation route;
The prepared bimodal systems have the potential to be used as contrast agents for optical and magnetic resonance imaging.
11

## Slide 12: Acknowledgment
12

## Slide 13
13
Thank you!!