## Slide 1
Agro-Industrial Waste Blends on Mechanical Response of Selected Soils
A paper presented at:
The 4th International Electronic Conference on Applied Sciences (ASEC 2023)
By
Imoh C. Attah,
George U. Alaneme,
Roland K. Etim,
Ahmad H. Jagaba,
Nimay C. Giri.
DATE: 27TH OCT – 10TH NOV 2023

## Slide 2: INTRODUCTION
The importance of road in the development of any nation can hardly be overemphasized, as it plays crucial role in the transportation of goods and services (Manasseh and Edeh, 2015).
During the construction of building, roads, railways, airfields, earth dams and fill for engineering projects, engineers are confronted with the challenge of quality construction materials especially where expansive soil is encountered.
Expansive soils are found in extensive deposits in the North Eastern part of Nigeria referred to as black cotton soils (BCS) are characteristically dark grey to black soil with high content of clay, usually over 50 % in which montmorillonite is the principal clay mineral (Morin, 1971).

## Slide 3: Introduction cont’d
In most cases, lateritic soil is used as subgrade, sub-base and base material for road construction purposes.
Considerable quantity of lateritic soil with ample clay content has the tendencies of affecting the strength and stability performance of the pavement structures (Oluwatuyi and Ojuri, 2017).
Expansive soils are soils with potential for shrinking or swelling under changing moisture condition (Fredlund and Rehardjo, 1993).
These BCS cause more damage to structures, particularly light building and pavements, than any other natural hazards, including earthquakes and floods (Jones and Holtz, 1973).

## Slide 4: Introduction cont’d
Calcium carbide powder (CCP) is a by-product from acetylene gas production.
Palm oil fuel residue (POFR) is a pozzolanic material that is obtained from palm oil waste incineration.
The use of CCP - POFR is as a result of the need for safe disposal of industrial and agricultural waste products due to the effect of these materials on the environment.
Huge quantities of waste materials from mineral, agricultural, domestic and industrial sources are generated daily, and the safe disposal of these wastes is increasingly becoming a major concern around the world (ETL, 1999).

## Slide 5: Aim and Objectives
The study is aimed at investigating the influence of calcium carbide powder – palm oil fuel residue on the mechanical response black clayey soil and reddish lateritic soil, respectively.
The specific objectives of this work include:
Determination of the physical properties of soil materials in their natural form.
Determination of Compaction characteristics.
Determination of California bearing ratio (CBR).
Determination of durability.
Micro fabric analysis.

## Slide 6: Materials
Soil sample (Black clayey soil and reddish lateritic soil)
Calcium Carbide Powder (CCP)
Palm oil Fuel Residue (POFR)

## Slide 7: Methods
Table 1 shows the list of tests carried out on the natural and treated soils in accordance with (BS1377, BS 1924, 1990) respectively.
Table 1: List of tests carried out
Physical Properties | Chemical and micro fabric | Mechanical Performance
Sieve analysis | Elemental composition | Compaction
Atterberg limit | Micro fabric analysis | California bearing ratio
Specific gravity |  | Durability
Moisture content |  | 

## Slide 8: Results Table 2: Properties of natural soil
Property of soil material | Quantity | 
 | BCS | RLS
Colour Percentage passing 75 μm | Greyish black 71.99 | Reddish brown 42.40
NMC; % | 20.20 | 15.74
Liquid Limit (%) | 56.30 | 49.30
Plastic Limit (%) | 27.60 | 20.50
Plasticity Index (%) | 28.70 | 28.80
Linear Shrinkage (%) | 18 | -
Free Swell (%) | 53.50 | -
Specific Gravity | 2.40 | 2.58
Optimum Moisture Content (%) | 18 | 13.1
Maximum Dry Density (Mg/m3) | 1.615 | 1.825
California Bearing Ratio (%) | 3 | 6
AASHTO Classiﬁcation (Group Index) | A-7-6 (14) | A-7-6 (20)
USCS Classiﬁcation | CH | SC

## Slide 9: Fig.1 Maximum Dry Density BCS-CCP-POFR
Chart: CCP Content (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 1.615 | 1.595 | 1.597 | 1.583 | 1.575 | 1.555
2 % POFR | 1.61 | 1.583 | 1.579 | 1.575 | 1.568 | 1.556
4 % POFR | 1.597 | 1.583 | 1.565 | 1.57 | 1.563 | 1.545
6 % POFR | 1.588 | 1.575 | 1.569 | 1.562 | 1.545 | 1.539
8 % POFR | 1.575 | 1.572 | 1.555 | 1.541 | 1.546 | 1.528

## Slide 10: Fig. 2 Maximum Dry Density RLS-CCP-POFR
Chart: CCP Content (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 1.825 | 1.795 | 1.784 | 1.772 | 1.765 | 1.748
2 % POFR | 1.819 | 1.788 | 1.789 | 1.77 | 1.76 | 1.732
4 % POFR | 1.81 | 1.776 | 1.77 | 1.762 | 1.75 | 1.74
6 % POFR | 1.799 | 1.768 | 1.757 | 1.748 | 1.74 | 1.715
8 % POFR | 1.781 | 1.767 | 1.75 | 1.74 | 1.727 | 1.695

## Slide 11: Fig. 3 Optimum Moisture Content BCS-CCP-POFR
Chart: CCP Content (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 18 | 18.4 | 18.45 | 18.68 | 19.3 | 19.25
2 % POFR | 18.35 | 18.6 | 18.7 | 19.15 | 19.45 | 19.2
4 % POFR | 18.65 | 18.9 | 19 | 19.1 | 19.45 | 19.5
6 % POFR | 18.8 | 19.1 | 19.3 | 19.35 | 19.6 | 19.6
8 % POFR | 18.9 | 19.35 | 19.5 | 19.6 | 19.75 | 20.15

## Slide 12: Fig 4 Optimum Moisture Content RLS-CCP-POFR
Chart: CCP Content (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 13.1 | 13.4 | 13.5 | 13.8 | 14 | 13.9
2 % POFR | 13.15 | 13.6 | 13.7 | 13.9 | 14.25 | 14
4 % POFR | 13.4 | 13.7 | 14 | 14.1 | 14.5 | 14.3
6 % POFR | 13.7 | 14 | 14.3 | 14.35 | 14.6 | 14.25
8 % POFR | 13.55 | 14.15 | 14.45 | 14.5 | 15 | 14.5

## Slide 13: Fig 5 CBR of BCS-CCP-POFR
Chart: CCP Content (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 3 | 8 | 6 | 13 | 18 | 14
2 % POFR | 5 | 11 | 12 | 17 | 19 | 18
4 % POFR | 9 | 9 | 16 | 18 | 25 | 21
6 % POFR | 12 | 13 | 15.5 | 24 | 27 | 25
8 % POFR | 14.5 | 16 | 19 | 23.5 | 27 | 30

## Slide 14: Fig 6 CBR of RLS-CCP-POFR
Chart: CCRContent (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 6 | 9 | 12 | 19.5 | 22 | 21
2 % POFR | 9 | 13 | 15 | 19 | 23 | 25
4 % POFR | 12 | 16 | 16 | 21 | 28 | 31
6 % POFR | 16 | 15.5 | 15.5 | 24 | 29 | 32
8 % POFR | 14 | 16 | 19 | 26.5 | 34 | 34

## Slide 15: Fig 7 Durability of BCS-CCP-POFR
Chart: CCR Content (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 9 | 14 | 16 | 17 | 24.4 | 19.9
2 % POFR | 13 | 17.4 | 18.2 | 19.8 | 26 | 25.8
4 % POFR | 18.4 | 19.1 | 19.6 | 23 | 32 | 25
6 % POFR | 17.3 | 22.5 | 22 | 28 | 28.8 | 32
8 % POFR | 24.5 | 24 | 28 | 30 | 37 | 39

## Slide 16: Fig 8 Durability of RLS-CCP-POFR
Chart: CCR Content (%)
| 0 | 3 | 6 | 9 | 12 | 15
0 % POFR | 11.5 | 16 | 18 | 19 | 25 | 24
2 % POFR | 16 | 19 | 19 | 23 | 28 | 31
4 % POFR | 20 | 18 | 23 | 22 | 32 | 33
6 % POFR | 23 | 23 | 26 | 28 | 35 | 31.5
8 % POFR | 24 | 30 | 29 | 37 | 38 | 41

## Slide 17: Fig. 9 Morphology of [a] unmodified BES [b] CCP-POFR modified BES

## Slide 18: Fig 10 Morphology of [a] unmodified BCS [b] CCP-POFR modified BES

## Slide 19: Conclusion
Judging from AASHTO, the marginal soil materials (BCS and RLS) in their unmodified form were categorized as A-7-6 (14) and A-7-6 (20) or CH and SC in USCS.
For both soil materials, the MDD displayed a downward trend with a corresponding increasing OMC on the incorporation of POFR-CCP blends.
The highest CBR values of 30 and 34 % for BCS and RLS was within the safe limit of 20 – 30 % as stated for sub-base material by the NGS.
The highest durability performance of the optimally modified soil materials were found to be 39 and 41 %, respectively.
The micro fabric assessment confirmed that the modified soils had morphological alteration.

## Slide 20
THANK YOU
FOR
LISTENING