## Slide 1
The 4th International Electronic Conference on Applied Sciences
CoFe2O4 spinel used as a catalyst for the degradation of organic dyes
K. DADDA1,*, S. DJERAD2
1Laboratoire des Matériaux Semi-conducteurs et Oxydes Métalliques (LMSOM), Faculté de Physique, Université des Sciences et de la Technologie Houari Boumediene Alger (USTHB), Algérie
2Laboratoire de Génie de l’Environnement, Depatement de Génie des Procédés. Université Badji Mokhtar Annaba (UBMA), Algérie
1,*daddakarima21@gmail.com
Abstract
Results
Conclusions
Fig.2: Rietveld refinement of the XRD pattern of the standard sample.
Table 1: crystal structure, lattice parameter (a), and crystallite size (< L >) of the standard (S) and alkaline (A) samples.
Fig.1: Evolution of the XRD diffractograms of the standard (S) and alkaline (A) samples.
Fig.3: FT-IR spectra of the standard (S) and alkaline (A) samples.
Ferrite powders were elaborated using the sol- gel process, the precursors are iron nitrate and cobalt nitrate. glycine was used as complexation and polymerization agent. The characterization techniques are X-ray diffraction (XRD) and Fourier Transform Infrared Spectroscopy (FT-IR).
The Rietveld refinement of the XRD patterns reveals the formation of the spinel ferrite cubic structure. Increasing the pH of the solution causes a slight change in the lattice parameter and crystallite size values.
FT-IR spectroscopy results confirm the formation of the spinel ferrite structure. Two types of metal oxygen bands are observed. The first type that appears for CoFe2O4 spectrum, in the range of 385 – 450 cm-1 , is attributed to the stretching vibrations of 𝐶𝑜2+− 𝑂 −2 ions. While the second type that appears in the range of 500 – 600 cm-1 is linked to intrinsic stretching vibrations of 𝐹𝑒3+ – 𝑂 2− ions.
Spinel ferrites have been widely studied owing to their structural, optical, dielectric, and magnetic properties leading to numerous applications. CoFe2O4 nanoparticles have been synthesized directly via the sol-gel method with glycine as a fuel. The Rietveld refinement of the X-ray diffraction patterns revealed the formation of a single cubic structure with a space group, no secondary phase was observed. The lattice parameter and the average crystallite size of powders produced from the standard and alkaline solutions were 8.36/8.38 Å, and 511/1060 Å, respectively. The characteristic vibrations modes of the spinel structure have been revealed by Fourier Transform Infrared spectroscopy. CoFe2O4 powders were tested for Fenton catalysis, and their performance was investigated for dye degradation.
1- XRD analysis
Experimental
The cobalt ferrite powders were prepared by the sol-gel method by mixing iron nitrates [Fe(NO3)3.9H2O], cobalt nitrates [Co(NO3)2.6H2O], and glycine [C2H5NO2] at the considered proportions. Nitrates were used as the oxidizers and the glycine as the fuel. The mixture were dissolved in 100 mL of dionized water. The first preparation of this mixture (standard, S) was heated at 100°C and the second one (alkaline, A) was regulated at pH = 11 by adding droplets of ammonia solution [NH4OH].
The two products were characterized by means of X-ray diffraction (PANalytical Empyrean diffractometer) and Fourier Transform Infrared Spectroscopy, FT-IR, (Spectrum two model FTIR spectrometer).
Sample | Space group | a (Å) | < L > (Å)
S | Fd-3m:1 | 8.36 | 511
A | Fd-3m:1 | 8.38 | 1060
The XRD patterns show well resolved and intensive diffraction peaks indicating a good crystallinity. The formation of CoFe2O4 type structure is confirmed by the presence of the most important diffraction peaks. The indexed (111), (220), (311), (222), (400), (422), (511), and (440) planes are in good agreement with those of the cobalt ferrite structures.
A
S
S
A
S
A
2- FT-IR analysis
385–450 𝑐𝑚-1 which is attributed to the stretching vibrations of 𝐶𝑜2+− 𝑂 −2 at octahedral sites.
3- Activity of spinel ferrites in the discoloration of methyle orange (MO)
Fig.4: Methyle orange oxidation by spinel ferrites.
FT-IR spectra of the synthesized ferrite powders reveal the characteristic peaks associated with the vibrations corresponding to cobalt and iron ions. In the wavenumber range of 385−450 cm-1 , the metal–oxygen bands are divided into two types: the first type, which is observed in the range of 500 – 600 𝑐𝑚-1 is due to intrinsic stretching vibrations of 𝐹𝑒3+ – 𝑂 2− ions in tetrahedral sites, while the second type in the range of
In oxic conditions, systems formed by metals/O2 may produce H2O2 in situ via the reduction of the dissolved oxygen in water by these metals. In this case, the oxidation of the metal and the reduction of oxygen occurred simultaneously:
M↔Mn++ne‒ and O2+2H++ 2e‒ ↔ H2O2
The formed Mn+ and H2O2 allows the implementation of Fenton process (an advanced oxidation process) thereby hydroxyl radicals are generated:
Mn++ H2O2 ↔ Mn+1+OH‒+ •OH
Hydroxyl radicals (•OH) with redox potential of 2.8 V are non-selective oxidants that aggressively attack all organic pollutants.
Increasing the pH of the solution improved the discoloration efficiency of MO. In fact, it increased from 64 to 91 % when the pH increased from 7 to 11 attained after 70 min of reaction.