## Slide 1
The 4th International Electronic Conference on Applied Sciences
27 Oct–10 Nov 2023 Online
Investigation of the structural and optical properties of ACZTS solid solution
Presented By:
KOUACI Khaled
Session: Applied Physical Science
Authors: Kouaci Khaled*1, 2, Belkhettab Ilyas2, Tablaoui Meftah2, Derbal Mourad1, Khelfane Amar2, Latreche Slimane3.

## Slide 2
Presentation outline
Introduction
Experimental details
Results and discussion
Conclusion
1
Notes: This presentation is structured as follows....

## Slide 3
Introduction
2
(Ⅰ2-Ⅱ-Ⅳ-Ⅵ4): Cu2ZnSn(S,Se)4
Iindirect bandgap
Intensive purification process
Toxicity of Cd
Scarcity and cost of Te
Scarcity and cost
of In and Ga
Elements from Group :
Ⅰ
Ⅴ
Ⅳ
Ⅱ
Ⅵ
Ⅲ
(Ⅳ): Si
(Ⅱ-Ⅵ): ZnS, CdTe
(Ⅰ-Ⅲ-Ⅵ2): Cu(In,Ga)Se2
Path from Si to quaternary chalcogenide (Ⅰ2-Ⅱ-Ⅳ-Ⅵ4) compound Semiconductors
Quaternary Chalcogenide Cu2ZnSnS4 material: Made from ecofriendly and abundant elements.
Large absorption coefficient ~ 104 cm-1. Direct band gap energy of about 1,5 eV.
Wide tunability of its structural and optical properties through elements substitution.
To focus on the effect of substituting Cu with Ag on the structural and optical properties of the solid solution (AgxCu1-x)2ZnSnS4 (ACZTS).
Diamond cubic
Zinc blende
Chalcopyrite
Kesterite

## Slide 4
Polycrystalline (AgxCu1-x)2ZnSnS4 x = 0.0 (AC00), 0.25 (AC25), 0.50 (AC50), 0.75 (AC75), 1 (AC100) have been synthesized via solid state reaction as follows :
Experimental details
Sealing a fused quartz ampoule loaded with raw material mixtures under vacuum
Heating the sealed ampoules to above the melting point of the compounds (980-1100°C)
Cooling the ampoule in a controlled manner by lowering the furnace temperature
retrieving the synthesized material
(ACZTS)
The temperature profile programmed in the electrical tubular furnace
3
Obtained ingot
AC75 sample

## Slide 5
Results and discussion
XRD powder analysis of the five synthesized
(AgxCu1-x)2ZnSnS4 ( 0 ≤ x ≤ 1) samples
For x=0 (CZTS), a distinct diffraction lines with the presence of main peaks at (112), (200), (220), (132) and (116) corresponding to the Kesterite CZTS structure.
The position of diffraction line shifts toward a low angles with the increase of Ag content.
As x=0.71, the (200), (220) and (312) start splitting up.
The dominant phase with a kesterite (CZTS) type-structure is gradually shifted into perquitasite-AZTS type structure.
As x=1 (AZTS), the (004), (204) and (116) peaks associated with tetrahedral perquitasite AZTS type structure appear.
Secondary phases, mainly (ZnS) in all compositions and others such as CuS, CTS in x=0 and SnS, SnS2 in x=1, are also revealed by XRD analysis.
4

## Slide 6
5
Lattice parameters trend of the obtained
(AgxCu1-x)2ZnSnS4 samples
The lattice parameters (a) and (c) of the obtained (AgxCu1-x)2ZnSnS4 samples as a function of ( 0 ≤ x ≤ 1) were calculated from the major peaks of XRD patterns ;
The lattice constant (a) increases slightly with increasing Ag content from x=0 to x=0.47, and when Ag ˃ 47% the lattice constant (a) undergoes a significant expansion, becoming considerably larger.
Similarly, the lattice parameter (c) increases slightly as we move from x=0 to x=0.47 compositions, while the latter parameter becomes significantly reduced beyond 47% Ag content.
The observed trends in lattice constants of (AgxCu1-x)2ZnSnS4 deviate from Vegard's law indicating the formation of point defects during synthesis.
Results and discussion

## Slide 7
6
Band gaps of (AgxCu1-x)2ZnSnS4 from diffuse reflectance spectroscopy measurements
Optical properties of (AgxCu1-x)2ZnSnS4, performed by UV-Vis diffuse reflectance measurements.
The optical properties could be tuned by varying the Ag content.
Due to the presence of secondary phases and points defects, the variation of the band gap does not depend linearly on Ag concentrations
Results and discussion

## Slide 8
Conclusion
7
The objective of this study was to prepare solid solutions of ACZTS by carefully following the steps of the solid state synthesis aiming to investigate the impact of the partial and total substitution of Cu by Ag on the properties of the CZTS absorber properties.
XRD powder analysis showed a noticeable pattern variation in the structural characteristics of the CZTS lattice. The diffraction lines are slightly shifted to lower angles with increasing Ag content, the perquitasite type AZTS structure peaks appeared in fully substituted compounds, implying that substitution of the Cu site by Ag occurs.
The lattice constants exhibit non-linear trends that deviate from Vegard's law as a consequence of defects formation during the synthesis, indicating that the formation of a solid solution within the (AgxCu1-x)2ZnSnS4 material did not occur as expected.
UV-Vis diffuse reflectance measurements showed that optical properties could be tuned by varying the Ag content, however, due to the presence of secondary phases, the variation of the band gap does not depend linearly on Ag concentrations.
Our results provide valuable insights into the effect of Ag substitution on the structural and optical properties of CZTS, and offer directions for further research into the nature of the defects observed in our samples, including additional characterization techniques namely XPS (X-ray photoelectron spectroscopy) and PL (photoluminescence)…
7

## Slide 9
THANK YOU

## Slide 10
References :
M. Tablaoui, M. Derbal, and K. Lebbou, “Discussion on the purity and the crystallization of CZTS compound,” J Cryst Growth, vol. 452, pp. 131–134, Oct. 2016, doi: 10.1016/j.jcrysgro.2016.04.008.
S. Alee, M. Asemi, M. Soltanmohammadi, and M. Ghanaatshoar, “Phase evolution studies of mechanochemical-prepared Cu2ZnSnS4powder via comprehensive annealing and milling investigation,” Powder Diffr, vol. 37, no. 1, pp. 22–33, Mar. 2022, doi: 10.1017/S0885715621000646.
Y. E. Romanyuk et al., “Doping and alloying of kesterites,” JPhys Energy, vol. 1, no. 4, Oct. 2019, doi: 10.1088/2515-7655/ab23bc.
A. Khelfane, M. I. Ziane, M. Tablaoui, M. Hecini, D. Ouadjaout, and M. Derbal, “Composition dependence of the optical band gap and the secondary phases via zinc content in CZTS material,” Inorg Chem Commun, vol. 151, p. 110639, May 2023, doi: 10.1016/j.inoche.2023.110639.