## Slide 1
Porous material for antimicrobial applications based on b-cyclodextrin and maltol derivative
V. Patamia, C. Zagni, V. Fuochi, S. Dattilo, S. Furnari, P. M. Furneri, G. Floresta, A. Rescifina

## Slide 2
Recently …

## Slide 3
Recently …

## Slide 4
Recently …

## Slide 5
AIM OF THE WORK
DRUG LOADING
IRON CHELATION CAPABILITIES

## Slide 6
SYNTHESIS
CRYO-POLYMERIZATION
Schematic diagram of cryogels synthetic procedure
T < 0 °C
Reactants
T > 0 °C
CRYOGELATION
10 µm
Monomer
Solutions
+ crosslinker
+ initiator
DEFROSTING
Solvent crystal
Porous

## Slide 7
SYNTHESIS

## Slide 8
SYNTHESIS

## Slide 9
SEM AND
POROSIMETRIC DISTRIBUTION

## Slide 10
IRON CAPTURE
-CD/HEMA/Malt
-CD/HEMA

## Slide 11
DRUG LOADING

## Slide 12
ANTIBACTERIAL ACTIVITY
WITHOUT

## Slide 13
ANTIBACTERIAL ACTIVITY
WITH
A) S. aureus
B) E. faecalis
C) P. aeruginosa
D) E. coli
E) K. pneumoniae
1) -CD/HEMA + Lomefloxacin
2) -CD/HEMA
3) -CD/HEMA/Malt + Lomefloxacin
4) -CD/HEMA/Malt
5) Lomefloxacin

## Slide 14
CYTOTOXICITY

## Slide 15
CONCLUSIONS
Fe3+
DRUG
A drug delivery system based on b-cyclodextrin-maltol derivative was designed
The material has optimal drug loading efficiency and iron chelation capabilities
Dual-acting antibacterial nanomaterial with lomefloxacin and iron depletion properties
No toxicity issue was reported in a human cell line

## Slide 16
THANKS FOR YOUR TIME
acknowledgements
Prof. Antonio Resciﬁna
Dr. Giuseppe Floresta
Dr.ssa Chiara Zagni
Dr.ssa Sabrina Carola Carroccio
Dr. Sandro Dattilo
Prof. Pio Maria Furneri
Dr.ssa Virginia Fuochi
Dr. Salvatore Furnari
GRAZIE
The research leading to these results has received funding from the European Union—NextGenerationEU under PNRR—M4C2-I1.3 Project “HEAL ITALIA”.