## Slide 1
AMINE OXIDE: SYNTHESIS AND ANALYSIS
NATIONAL UNIVERSITY OF OIL AND GAS «GUBKIN UNIVERSITY»
The 28th International Electronic Conference on Synthetic Organic Chemistry
Presented by: Mityurev Savely Alekseevich
Faculty of chemical and environmental engineering
Prepared by: M.A. Silin, L.A. Magadova, P.K. Krisanova,
M.M. Muhin, S.A. Borodin, A.A. Filatov, S.A. Mityurev
the scientific staff of the Department of Technology
of Chemicals for Oil and Gas Industry
Bachelor of the Department of Technology
of Chemicals for or Oil and Gas Industry

## Slide 2
Scientific work relevance and problematics
Methods
Results and discussion
Conclusion
Introduction
Performance plan

## Slide 3
Surfactants and fracking
Oil and Gas
rich layer
Oil and Gas
three-dimensional grid structure
surfactant molecules
cylindrical
micelle
spherical micelle

## Slide 4
Light organochlorine compounds (LOC)
technological equipment corrosion
deposits on processing units
catalyst
deactivation
NO LOC
–
+
Non-polar hydrophobic (water-hating) tail
Polar hydrophilic (water-loving) head

## Slide 5
Research subject
“Amine Oxide”
(oleylamidopropyldimethylamine oxide – OADAO)
feasible industrial production in Russia
high stability
resistance to the impact of microorganisms
easy availability of raw materials
light organochlorine compounds absence in the synthesis
high degree of biodegradability

## Slide 6
Potentiometric titration | Calculated value
36,93 % | 38,34 %
Synthesis results and Research methods
Fourier transform infrared spectrometer
(Thermo Scientific Nicolet iS10)
Rotary evaporator (Labtex IR-1LT)
Evaporative flask
Warming bath
Control panel
Reflux condenser
Receiving flask
Motor
Sample feed tap
pH meter
(S20 SevenEasy Mettler Toledo)
Solvent | t, °C | τ, h | Characteristic features
– | 60 | 5-6 | abundant foam formation
PEG | 0,5000 |  | 43,33%
i-C3H8O |  |  | no foam at all
Synthesis conditions
Mass content of the amine oxide

## Slide 7
3292 cm-1
IR absorption spectra (FTIR)
Absorbance
Wave number, cm-1
0,32
0,30
0,28
0,26
0,24
0,22
0,20
0,18
0,16
0,14
0,12
0,10
0,08
0,06
0,04
0,02
0,00
1500
1000
2000
2500
3000
3500
End-product
Initial amine
968 cm-1
929 cm-1
Absorbance
Wave number, cm-1
0,16
0,15
0,14
0,13
0,12
0,11
0,10
0,09
0,08
0,07
0,06
0,05
0,04
0,03
0,02
0,01
0,00
1500
1000
1644-1650 cm-1
End-product
Initial amine
Wave number, cm-1 | Chemical bond
968 and 929 | N→O
3292 | O–H
1650–1644 | C=O

## Slide 8
Conclusion:
IR-Fourier spectroscopy and potentiometric titration confirm the successful synthesis;
The mass content of OADAO in the reaction mass at the end of synthesis is approximately 37 %. The calculated and experimental data are consistent;
Amine oxide can simultaneously exist in the solution in two ionic forms, which is confirmed by the obtained IR spectra
Way forward:
variation temperature and duration of the synthesis
Current research outcomes:
research the influence of synthesis conditions on the yield of end-product
develop the most appropriate synthesis technique
investigation of amine oxide as a gelling agent of fracturing fluids on a water basis