## Slide 1: Nanotechnology to improve the performances of hydrodynamic surfaces
Ali ALSHEHRI,
El Hadj DOGHECHE, Laurent KEIRSBULCK., Philippe Champagne

## Slide 2: OUTLINES
Introduction (Maritime industry challenges)
Project Strategy
Super-Hydrophobic Surfaces (Potential solution, Conditions & Publications)
Market Studies
Proposed Solutions
Achievements
Conclusion

## Slide 3: contexte
  Corrosion ($276 billion for usa/YAER = 3.1% of usa gdp) *
  Fouling ($150 billion / year 2020 globe ) **
  Energy
  Environment (2001, IMO Convention prohibit TBT) ***
  Hydrodynamic performances
* J. H. P. Gerhardus, “Corrosion Costs and Preventive Strategies in the United States,” NACE Int., pp. 3–11, 2002.
** C. Hellio and D. Yebra, Advances in marine antifouling coatings and technologies. Woodhead Publishing Limited, 2009.
*** TBT (Tributyltin)

## Slide 4: Objective
  enhance the maritime surfaces CHARACTERISTICS BY Super hydrophobic treatment
(WCA) (θ) ≥ 150°
Sliding Angle (SA) (α) ≤ 10°
α
α: Sliding Angle (SA)
θ
Solid
Liquid
θ: Water Contact Angle (WCA)

## Slide 5: Super hydrophobic Coating (Publications)
Chart: Superhydrophobic Coating
| 2018 | 2017 | 2016 | 2015 | 2014 | 2013 | 2012 | 2011 | 2010 | 2009 | 2008 | 2007 | 2006 | 2005 | 2004 | 2003 | 2002 | 2001 | 2000 | 1999 | 1998
Superhydrophobic Coating | 9150 | 8320 | 7180 | 5980 | 5380 | 4630 | 3780 | 3390 | 2500 | 2240 | 1760 | 1190 | 887 | 554 | 337 | 205 | 143 | 96 | 92 | 50 | 40

## Slide 6: strategy
Market study
Creation of Super Hydrophobic surfaces
Hydrophobic test
Hydrodynamic tests

## Slide 7: strategy
Market study
Creation of Super Hydrophobic surfaces
Hydrophobic test
Hydrodynamic tests

## Slide 8: Market Studies
Water Contact Angle (WCA)
Sliding Angle (SA)
Sliding speed (Vs)
Surface morphology
Energy-dispersive X-ray (EDX)
Surface tension (ST)
Surface roughness (RA)
Ø = 100 mm
Primer (Pr), 40µm
Anti Corrosion (AC), 150µm
Tie Coat (TC), 100µm
Classic Antifouling (AF),150µm
Primer (Pr), 40µm
Epoxy, 250µm
Epoxy
paint system
Classic A.F.
paint system
Silicone A.F.
paint system
Primer (Pr), 40µm
Anti Corrosion (AC), 150µm
Tie Coat (TC), 100µm
Silicone Antifouling (AF),150µm
configuration of paint layers

## Slide 9: Epoxy Paint
Element | Weight % | Atom %
Al | 0.28 | 0.42
S | 1.12 | 1.43
Mg | 2.03 | 3.42
Si | 3.40 | 4.95
Cl | 8.91 | 10.27
Fe | 10.68 | 7.81
O | 13.00 | 33.19
Zn | 24.21 | 15.13
Cu | 36.37 | 23.38
Total | 100.00 | 100.00
Surface morphology
EDx
Ra = 373 (nm)
Confocal microscopy
WCA = 85°
SA = 36°
ST= 43 (mJ.m-²)
Vs = 0.23 m/s

## Slide 10: Classic A.F. Paint
Element | Weight % | Atom %
Ca | 0.70 | 0.47
Cl | 1.69 | 1.30
Fe | 6.55 | 3.20
S | 7.73 | 6.59
Mg | 10.15 | 11.41
Si | 19.86 | 19.31
Ba | 22.09 | 4.39
O | 31.23 | 53.32
Total | 100.00 | 100.00
Surface morphology
Confocal microscopy
Ra = 923 (nm)
WCA = 84°
SA = 37°
ST= 43 (mJ.m-²)
EDx
Vs = 0.16 m/s

## Slide 11: Silicone A.F. Paint
Element | Weight % | Atom %
Fe | 2.43 | 0.99
O | 33.22 | 47.07
Si | 64.35 | 51.95
Total | 100.00 | 100.00
Confocal microscopy
Ra = 121 (nm)
WCA = 101°
SA = 16°
ST= 23 (mJ.m-²)
Surface morphology
EDx
Vs = 0.3 m/s

## Slide 12: Market Studies
WCA = 101°
SA = 16°
ST= 23 (mJ.m-²)
SS = 0.3 m/s
Epoxy
paint system
25€/L
Silicone A.F.
paint system
75€/L
Classic A.F
paint system
40€/L
Lotus Leaf : WCA=153.4°,SS = 0.32 m/s
WCA = 84°
SA = 37°
ST= 34 (mJ.m-²)
SS = 0.16 m/s
WCA = 85°
SA = 36°
ST= 43 (mJ.m-²)
SS = 0.23 m/s

## Slide 13: strategy
Aluminum
Epoxy
ZnO + ODS
Market study
Creation of Super Hydrophobic surfaces
Hydrophobic test
Hydrodynamic tests

## Slide 14: Proposed Solutions
Create Super-Hydrophobic Surfaces from Nanotechnology Process
ZnO NRS nanorods by Hydrothermal process (antibacterial, simple fabrication & green material: most popular solution studied (0.5 M Paper 2007-2017)
reduce surface energy ODS (OctaDecyltrimethoxySilane)

## Slide 15: protocol
1. ZnO seeds
3. ODS
2. ZnO NRs

## Slide 16
seeds

## Slide 17
ZnO NRs

## Slide 18: strategy
Market study
Creation of Super Hydrophobic surfaces
Hydrophobic test
Hydrodynamic tests

## Slide 19: CHARACTERIZATION (wca & sa)
α
α: Sliding Angle (SA)
θ
Solid
Liquid
θ: Water Contact Angle (WCA)
DSA25S, Kruss

## Slide 20: CHARACTERIZATION (aluminium + epoxy) (wca & sa)

## Slide 21: strategy
Market study
Creation of Super Hydrophobic surfaces
Hydrophobic test
Hydrodynamic tests

## Slide 22: CHARACTERIZATION (Sliding Speed) (sS)
Sliding Speed (SS)
90°
50µl
Aluminium substrat
Epoxy Paint
D = 100mm
90°
50µl
Aluminium substrat
Epoxy Paint
100mm
T= t
T= t + Δt

## Slide 23: CHARACTERIZATION (aluminium + epoxy) (sS)
Sliding Speed (SS)
90°
50µl
Aluminium substrat
Epoxy Paint
D = 100mm
Chart: Distance (m)
| 0.02 | 0.03 | 0.04 | 0.05 | 0.06 | 0.07 | 0.08 | 0.09
(a) Aluminum | 0.060772 | 0.098223 | 0.12011 | 0.14617 | 0.17612 | 0.21308 | 0.22222 | 0.24894
(b) Epoxy | 0.01358 | 0.012244 | 0.018097 | 0.018536 | 0.023223 | 0.028877 | 0.025902 | 0.036712
(c) ZnO+ODS | 0.43116 | 0.64167 | 0.78846 | 0.88636 | 0.94545 | 1.1111 | 1.125 | 1.3036

## Slide 24: CONCLUSION
MARKET STUDy.
  Best WCA, SA & sliding speed (WCA +20%) (SA -55%) (Vs +14%): Silicone paint
ACHIVEMENTs.
  WCA >152°, sa < 7°
  Perspectives:
    Application naca airfoil
    characterizations: fouling, antibacterial, resistance & Duration.