## Slide 1
Microencapsulation of bioactive leaf extracts of Eucalyptus camaldulensis by freeze drying technology using sodium alginate and sodium carboxymethyl cellulose as coating materials
Ozioma Forstinus Nwabor1 and Supayang Piyawan Voravuthikunchai1*
1Excellence Research Laboratory on Natural Products, Department of Microbiology, Faculty of Science and Natural Product Research Center of Excellence, Prince of Songkla University, Hat Yai, Songkhla, 90112, Thailand
* supayang.v@psu.ac.th, nwaborozed@gmail.com

## Slide 2
Microencapsulation of bioactive leaf extracts of Eucalyptus camaldulensis by freeze drying technology using sodium alginate and sodium carboxymethyl cellulose as coating materials

## Slide 3
Abstract:
Bioactive crude ethanolic extracts of Eucalyptus camaldulensis was encapsulated with alginate–CMC using freeze drying technique. The microcapsules were characterized for particle size, morphology, physicochemical parameters such as solubility, swelling index, and micromeritics properties. FTIR was used to evaluate the interactions of the polymer and the extract. Antioxidant and antimicrobial activities of the microcapsules were also demonstrated. Results revealed and irregular shaped microparticles with mean diameter ranging from 6.7–26.6 µm. Zeta potential and polydispersity index ranged from -17.01–2.23 mV and 0.344–0.489 respectively. Percentage yield and encapsulation efficiency ranged between 70.4–81.5 % and 74.2±0.011 – 82.43±0.772 %. In addition, the microcapsules exhibited high swelling index with poor solubility. Antioxidant activity of the microcapsules evaluated using DPPH and ABTS assays increased with increase in the concentration of the extract. Minimum inhibitory and minimum bactericidal concentrations of the microcapsules against gram-positive foodborne pathogens ranged from 0.19–3.12 mg/mL and 0.19–12.25 mg/mL respectively. Moreover, the microcapsules at concentration of 1 mg/mL did not show cytotoxic effects on human colon cell CaCo-2. Alginate–CMC showed good encapsulation properties that preserved the bioactivity of the extract, thus might be employed for application of natural products in processing systems.
Keywords: Microencapsulation; Freeze–drying; Eucalyptus camaldulensis; Bioactive; Cytotoxicity

## Slide 4
Introduction
Plants are excellent source of bioactive, natural and healthy compounds that could be used in product formulation
However, the inert nature of most of these bioactive compounds limits their usage
Microencapsulation as a technique preserves plant component active compounds, resulting in prolonged activity, as well as regulated release
Alginate and carboxymethyl cellulose are both biocompatible polymers with wide usage in the food industry

## Slide 5
Eucalyptus a plant native to Australia and the Southeast Asia contains various phytochemicals and is a rich source of medicinal essential oil
Leaf extracts of the plant have been reported to exhibit good antimicrobial and antioxidant activities
Leaf extracts of the plant was microencapsulated by freeze-drying technique, characterized and assessed for bioactive activities

## Slide 6
Results and discussion
Formulations | Particle Size (µm) |  |  | 
 | D10 | D50 | D90 | Span
F0 | 3.07 | 6.70 | 14.63 | 1.73
F1 | 11.85 | 26.59 | 59.70 | 1.79
F2 | 4.99 | 10.03 | 20.15 | 1.51
F5 | 4.41 | 9.06 | 18.61 | 1.56
Table 1, shows the particle size of microcapsules reported based on equivalent sphere concept (D10: 10th percentile of cumulated volume distribution, D50: median particle diameter (50th percentile) of cumulated volume distribution and D90: 90th percentile of cumulated volume distribution) and span.
The D50 values of the microcapsules ranged from 6.7–26.6 µm, with the blank microcapsules presenting the lowest particle size of 6.7 µm.
TABLE 1

## Slide 7
From Table 2, a high percentage yield (70.4–81.5%) was observed, demonstrating a minimal loss of material. Similarly, encapsulation of the extract using alginate–CMC demonstrated %EE of 74.2±0.011–82.43±0.772%, suggesting the formation of stable interactions between reactive sites of the polymers and the extract.
In addition, the alginate–CMC encapsulated extract showed a zeta potential of -11.01, -17.01, 2.23 and -2.45 for F0, F1, F2 and F5 respectively with , PDI ranging between 0.344–0.489, indicating a wide size dispersion.
TABLE 2
Formulations | % Yield | Encapsulation efficiency (%) | Swelling index (%) | Polydispersity index | Zeta potential (mV) | Solubility (%)
F0 | 80.7 | NA | 84.0 | 0.450 | -11.01 | 22.2±1.1
F1 | 76.5 | 74.2 ± 0.011 | 81.4 | 0.489 | -17.01 | 22.1±1.6
F2 | 81.5 | 80.11 ± 0.008 | 71.8 | 0.344 | 2.23 | 19.9±0.1
F5 | 70.4 | 82.43 ± 0.772 | 54.4 | 0.370 | -2.45 | 18.8±0.2

## Slide 8
Table 3, shows the antimicrobial activities of the encapsulated extracts of E. camaldulensis against foodborne pathogenic bacteria. The microencapsulated extracts demonstrated antimicrobial effects with minimum inhibitory concentrations and minimum bactericidal concentrations ranging from 0.19–3.12 and 0.19–12.25 mg/mL.
TABLE 3
Isolates | MIC/MBC (mg/mL) |  |  |  | 
 | Blank | F1 | F2 | F5 | Extract
Bacillus cereus | >24 | 0.39/1.56 | 0.19/0.39 | 0.19/0.19 | 0.064/0.128
Listeria monocytogenes | >24 | 1.56/6.25 | 0.39/6.25 | 0.19/0.78 | 0.128/0.512
Staphylococcus aureus | >24 | 3.12/12.25 | 1.56/6.25 | 0.39/1.56 | 0.128/0.256

## Slide 9
FIGURE 1
The FTIR spectra showing interactions at the C-H peak located at 2928 cm-1 and 2950 cm-1 in the extract and blank capsules, resulting in a minor shift to 2926 cm-1.

## Slide 10
FIGURE 2
The antioxidant activities of the microcapsules, demonstrated using the (A) DPPH and (B) ABTS assays. The capsules showed a concentration dependent inhibition with F5 showing the highest antioxidant properties and F1 the least antioxidant activity

## Slide 11
FIGURE 3
The total phenolic and flavonoid contents of the microcapsules are presented in (Figure 3). The results indicate a TPC content of 0.26, 0.15, and 0.09 mg garlic acid equivalent/mg sample for formulation F5, F2 and F1 and a TFC of 0.21, 0.09 and 0.06 mg catechin equivalent/mg sample for F5, F2 and F1

## Slide 12
FIGURE 4
Morphological examination of the microcapsules by scanning electron microscopy showed irregular shape and compact structure similar to previously observed micrograph for freeze dried microcapsules.

## Slide 13
FIGURE 5
Cytocompatibility testing of microcapsules
The cytotoxicity evaluation of eluates obtained from microcapsules at various time intervals against human embroyonic colon cell Caco–2 showed >80% cell viability when compared with the control (100%). Encapsulation of active compounds can reduce the adverse effects through regulated slow release with prolonged activity.

## Slide 14
Conclusions
Freeze drying methods yielded microcapsules with good properties
Sodium alginate and sodium carboxymethyl cellulose co-polymers should good properties as encapsulants with excellent encapsulation efficiency and percentage yield
The capsules should high retention of the core as shown by the TPC and TFC contents
The microcapsules exhibited antimicrobial and antioxidant properties reflecting the release of the core material

## Slide 15
Conclusions
Scanning electron microscopy revealed irregular microcapsules
The microcapsules showed excellent compatibility with human embryonic colon cell Caco-2

## Slide 16
Acknowledgments
This work was supported by Thailand’s Education Hub for ASEAN Countries (Grant No. TEH-AC 013/2017) and TRF senior Research Scholar (Grant no. RTA 6180006), the Thailand Research Fund.