## Slide 1
Development of new catalytic material for accurate detection of biological biomarkers related to most common Non-communicable diseases
Ana Moraisa,b, Marisa Nicolaia, Belén Bataneroc, Patrícia Rijoa,d
                a CBIOS - Center for Research in Biosciences & Health Technologies, Universidade Lusófona de Humanidades e Tecnologias, Campo Grande 376, 1749-024 Lisboa, Portugal.
                b Department of Biomedical Sciences, Faculty of Pharmacy, University of Alcalá, Ctra. A2, Km 33.600 – Campus Universitario, 28871 Alcalá de Henares, Spain.
                c Department of Organic & Inorganic Chemistry, Faculty of Pharmacy, University of Alcalá, Spain; belen.batanero@uah.es
                d iMed.ULisboa - Instituto de Investigação do Medicamento, Faculdade de Farmácia, Universidade de Lisboa, 1649-003 Lisboa, Portugal.
State of Art of Non-communicable disease
Plasma membrane
Peroxisomes
NAD(P)H Oxidase Lipoxygenase Cyclooxygenase Xanthine oxidoreductase Cytochrome P450 NADH COQ reductase Cytochrome c oxidase Dehydrogenases
Mitochondrion
Endoplasmic reticulum
Nucleus
NON
COMMUNICABLE
DISEASES
Cardiovascular condition
Chronic respiratory condition
Cancer
Diabetes
ROS
mitochondrial metabolism
organelles response
Activation of [1]
Oxidative stress
Interfering with cellular biological processes
Proteins structure/activity
DNA strands damaging
Phospholipid membranes permeability disruption
Protective mechanism
Capture/ linkage with ROS
Recover physiological processes
Inhibits ROS oxidative action
Antioxidant species
► Early diagnosis ►Health management
Electrochemical sensing[2]
Biosensor sensitivity relies on electrode catalytic activity over electroactive species of analyte
Choice of catalytic material is of utmost importance for electrochemical biosensors.
NPs suited[3] Pharmaceutical & Biochemical industry
Metal ion is reduced to its atomic zero-valence state
cluster nucleation growth atom
clusters stabilization
capping growth
metal cation
nucleation
Bulk Powder Nanostructure
High surface – area – to - volume ratio
Nano-size to wavelength of an electron
Nano-materials
Nanoparticles readily interact with eukaryotic cells [2]
Figure 1: Nanoparticles crossing membrane cells barrier: by endocytosis /diffusion
Conventional synthesis wet-chemical method
Precursor salt aqueous sol.
Reducing agent + Stabilizer
NP synthesis
Harmful
Phytochemical species usually trend to donate electrons to seeking electron species, behaving as anti-oxidant.
Figure 2: Plectranthus Cilliatus & Plectranthus Rosmarinus Officinallis species
Phytonutrients are the most commonly used Eukarya-domain reducing agents
Flavonoids
Terpenoids
Alkaloid
Gives electrons to metallic anions turns them into their zero-valence atomic state[4]
Plectranthus genus plant-extract reduction of provides high stabilized well-dispersed spherical Ag NPs[5].
Plant-base Biogenesis
Hydrazine Hydrate (Phenilhydrazine)
Ascorbic Acid
Sodium Borohydride
Sodium Citrate
Reduce agent | Average particle size/nm | Zeta potential/mV
NaBH4 | 180 | -29
P. R. Officinalis | 198 | -26
P. Ciliatus | 409 | -30
Table 1: Physicochemical evaluation of prepared silver nanoparticles.  particle size (Dynamic Light Scattering) & zeta potential (Electrophoretic Light Scattering)
Figure 2: Mean particle size, polydispersity index (top bars) and zeta potential (bottom bars) characterisation of synthesised Ag nanoparticles (n = 3, mean ±SD)
NaBH4
Rosemary officiallis extract as reducing agent
Plenctractus ciliatus extract
AgNPs
Figure 3: Aqueous colloid of biosynthesized Ag NPs
[1] Morais, A.L.; Rijo, P.; Batanero, B.; Nicolai, M. Biomolecules and Electrochemical Tools in Chronic Non-Communicable Disease Surveillance: A Systematic Review. Biosens (accepted 7 September 2020).
[2] Morais, A.L.; Salgado, J.R.C.; Šljukić, B.; Santos, D.M.F; Sequeira, C.A.C. Electrochemical behaviour of carbon supported Pt electrocatalysts for H2O2 reduction, Int. J. Hydrog. Energy. 2012; Volume 37, pp. 14143–14151.
[3] Ullah Khan S.; Saleh T.A.; Wahab A.; Khan U.; Khan D.; Ullah W.; Rahim A.; Kamal S.; Ullah K.F.; Fahad S.; Nanosilver: new ageless and versatile biomedical therapeutic scaffold. Int J Nanomedicine. 2018; Volume 13, pp. 733–762.
[4] Zheng, Y.; Huang, Y.; Shi, H.; Fu, L. Green biosynthesis of ZnO nanoparticles by plectranthus amboinicus leaf extract and their application for electrochemical determination of norfloxacin. Inorg Nano-met Chem. 2019; Volume 49, pp. 277–282.
[5] Ajitha, B., Ashok Kumar Reddy, Y., & Sreedhara Reddy, P. Biosynthesis of silver nanoparticles using Plectranthus amboinicus leaf extract and its antimicrobial activity. Spectrochim. Acta A Mol. Biomol. Spectrosc. 2014; 128, 257–262.
Dodecanoic saturated fatty acid
SDS surfactant
Triton x-100 surfactant
reducing agent
Long chain stabilizers
Harmful
Therapeutic / Diagnosis Nanotechnology
Nanomaterial on drug delivery therapy
Nanomaterial on Accurate Diagnosis