## Slide 1
Quantum chemical modeling of molecular crystal deformations
Yevhenii A. Vaksler 1,2,3,*, Abdenacer Idrissi 2, and Svitlana V. Shishkina 1,3
1 V.N. Karazin Kharkiv National University, 4 Svobody Sq., Kharkiv, 61022, Ukraine
2 SSI “Institute for Single Crystals” NAS of Ukraine, 60 Nauky ave., Kharkiv, 61001, Ukraine
3 Laboratoire de Spectroscopie pour les Interactions, la Réactivité et L’environnement (UMR CNRS A8516), Université de Lille, 59655, Villeneuve d’Ascq Cedex, France.
* Corresponding author: vakslerea@gmail.com

## Slide 2: Energy-vector diagrams for visualization

## Slide 3: Energy-vector diagrams for visualization
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule

## Slide 4: Energy-vector diagrams for visualization
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule
- van der Waals radius of the j atom of the neighboring molecule

## Slide 5: Energy-vector diagrams for visualization
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule
- van der Waals radius of the j atom of the neighboring molecule

## Slide 6: Energy-vector diagrams for visualization
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule
- van der Waals radius of the j atom of the neighboring molecule

## Slide 7: Energy-vector diagrams for visualization
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule
- van der Waals radius of the j atom of the neighboring molecule

## Slide 8: Energy-vector diagrams for visualization
Length of the vector:
where Rn – the distance between the geometric centers of nth neighbor and the initial molecule
En – interaction energy between between nth neighbor and the initial molecule
Estr – energy of the strongest pairwise interaction in crystal
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule
- van der Waals radius of the j atom of the neighboring molecule

## Slide 9: Energy-vector diagrams for visualization
Length of the vector:
where Rn – the distance between the geometric centers of nth neighbor and the initial molecule
En – interaction energy between between nth neighbor and the initial molecule
Estr – energy of the strongest pairwise interaction in crystal
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule
- van der Waals radius of the j atom of the neighboring molecule

## Slide 10: Energy-vector diagrams for visualization
Length of the vector:
where Rn – the distance between the geometric centers of nth neighbor and the initial molecule
En – interaction energy between between nth neighbor and the initial molecule
Estr – energy of the strongest pairwise interaction in crystal
Search for neighbors:
where Dij – distance between the i and j atoms of the initial molecule and nth neighbor
- van der Waals radius of the i atom of the initial molecule
- van der Waals radius of the j atom of the neighboring molecule

## Slide 11: Classification of molecular crystals
Isotropic
Columnar
Layered
Columnar-layered
Shishkin O. V. , Zubatyuk R. I., Shishkina S. V., [et al.] (2014).
Phys. Chem. Chem. Phys., 16, 6773-6786.
Relationship between anisotropy of physical properties and anisotropy of crystal packing
Different properties of polymorphs due to different systems of intermolecular interactions

## Slide 12: Aspirin’s polymorphic forms
4
Shtukenberg A., Hu C., Zhu Q., [et al.] (2017).
Cryst. Growth Des., 17(6), 3562-3566
P21/c: a= 16.741, b= 4.795, c= 23.802 β= 111.08
III
Unknown form
P21/c: a= 11.2776, b= 6.5517, c= 11.2741 β= 95.837
I
III
2.0 GPa
P21/c: a= 12.1515, b= 6.5064, c= 11.3677 β= 111.574
II
III
2.2 GPa
Bond A., Boese R., Desiraju G. (2007).
Angew. Chem. Int. Ed., 46(4), 615-617
Pressure
drop
Metastable
Grinding*
*Varughese S., Kiran M. S. R. N., Solanko K. A., [et al.] (2007).
Angew. Chem. Int. Ed., 46(4), 615-617

## Slide 13: Analysis of energetic structure of aspirin’s polymorphs
5
Interaction energy, kcal/mol | I |  | II |  | III AA |  | III BB | 
 | (1 0 0) | (0 0 1) | (1 0 0) | (-1 0 2) | (1 0 0) | (0 0 1) | (1 0 0) | (0 0 1)
In chain | -26.8 |  | -26.9 |  | -35.3 |  | -32.9 | 
Between chains in layer | -32.2 | -12.3 | -33.6 | -13.3 | -19.7 | -17.4 | -20.9 | -17.4
In layer | -59.9 | -39.0 | -60.5 | -40.1 | -55.0 | -52.8 | -53.8 | -50.3
Between layers | -15.4 | -36.3 | -14.8 | -35.2 | -24.6 | -26.9 | -24.6 | -28.1
Chain with all neighbors | -48.6 |  | -48.4 |  | -44.3 |  | -45.5 | 
Total | -73.5 |  | -73.5 |  | -79.7 |  | -78.5 | 
I
II
III

## Slide 14: Modelling of shift in aspirin’s crystals
6
 | Shift energy barrier, kcal/mol | Minimal distance, Å
I [001] (100) | 17.1 | 1.19
II [001] (100) | 14.5 | 1.27
III [010] (001) | 9.2 | 1.73
III [010] (100) | 5.3 | 1.73
III [010] (-101) | 8.5 | 1.82
Crystal structure transformation under pressure

## Slide 15
7
Transformation in piracetam under pressure
Tableting
Pressure growth
1 bar
0.45 GPa
0.70 GPa
Conversion
0.90 GPa
2.50 GPa
4.00 GPa
?
Form II, P-1: a= 6.321, b= 6.5597, c= 8.380
α= 79.82, β= 102.34, γ= 90.94
Form V, P-1: a= 6.442, b= 6.3530, c= 8.737
α= 81.43, β= 112.88, γ= 91.38
Fabbiani F. P. A., Allan D. R., David W. I. F., [et al.] (2007).
Cryst. Growth Des., 7(6), 1115-1124.

## Slide 16
8
Changes in energetic structure of piracetam upon a transition
Interaction energy, kcal/mol | II at 0.45 GPa |  |  | V at 0.70 GPa |  | 
 | (001) | (010) | (0-11) | (001) | (010) | (0-11)
In chain | -35.9 |  |  | -34.6 |  | 
Between chains in layer | ‑19.2 | ‑8.8 | ‑9.6 | ‑20.4 | ‑13.2 | ‑12.9
In layer | ‑74.3 | ‑53.4 | ‑55.2 | ‑75.4 | ‑60.9 | ‑60.3
Between layers | ‑18.4 | ‑28.8 | ‑27.9 | ‑26.0 | ‑33.2 | ‑33.5
Total | -111.0 |  |  | -127.4 |  | 

## Slide 17
9
Modelling of shift in piracetam’s crystals
Polymorph | Pressure, GPa | Shift energy barrier, kcal/mol | Minimal distance, Å
II | 1.00*10-4 | 5.3 | 1.72
 | 0.45 | 6.0 | 1.84
V | 0.70 | 7.2 | 2.01
 | 0.90 | 8.2 | 1.96
 | 2.50 | 9.4 | 1.88
 | 4.00 | 10.3 | 1.84
[100] direction along (001) layer

## Slide 18
10
Cavities detection in piracetam
Shortening of the van der Waals radii sum at a point:
-
where – the distance between the atoms of fixed (i) and motile (j) parts
– van der Waals radii of the corresponding atoms in fixed (i) and motile (j) parts

## Slide 19
10
Cavities detection in piracetam
(0.78,0.97)
Shortening of the van der Waals radii sum at a point:
-
where – the distance between the atoms of fixed (i) and motile (j) parts
– van der Waals radii of the corresponding atoms in fixed (i) and motile (j) parts

## Slide 20
11
Comparison of structure and energy assessment of the transition in piracetam crystals
Polymorph II under the pressure of 0.45 GPa
Polymorph V under the pressure of 0.70 GPa

## Slide 21
11
Comparison of structure and energy assessment of the transition in piracetam crystals
(0,0): -16.4 kcal/mol
(0.78,0.97): -9.0 kcal/mol
No repulsion!
Polymorph II under the pressure of 0.45 GPa
Polymorph V under the pressure of 0.70 GPa

## Slide 22
11
Comparison of structure and energy assessment of the transition in piracetam crystals
Compression
Polymorph II under the pressure of 0.45 GPa
Polymorph V under the pressure of 0.70 GPa
(0,0): -16.4 kcal/mol
(0.78,0.97): -9.0 kcal/mol
No repulsion!

## Slide 23
12
Consistency of ibuprofen’s structure
Ostrowska K., Kropidłowska M., Katrusiak A. (2015)
Cryst. Growth Des., 15(3), 1512-1517.
No conversion
under pressure!
Compression up to 4 GPa

## Slide 24
Sustainability of ibuprofen’s energetic structure
Interaction energy, kcal/mol | 0.23 GPa |  | 
 | (100) | (001) | (102)
In chain | -21.6 |  | 
Between chains in layer | ‑30.3 | ‑6.0 | ‑4.5
In layer | -82.2 | -33.6 | -30.5
Between layers | ‑10.5 | ‑34.8 | ‑36.3
Total | -103.2 |  | 
13
Total energy
Energy in layer

## Slide 25
14
Modelling of shift in ibuprofen’s crystals
Pressure, GPa | Shift energy barrier, kcal/mol | Minimal distance, Å
0,23 | 13,6 | 1,46
0,60 | 24,9 | 1,30
0,80 | 34,8 | 1,18
0,88 | 34,7 | 1,20
2,65 | 104,6 | 0,86
4,00 | 190,7 | 0,70
9.1 kcal/mol
0.40
[001] direction along (100) layer

## Slide 26
15
Conclusions
On the base of a study of pairwise interactions energies in crystals the new quantum-chemical method able to describe shear-based transformations of crystal structures was proposed.
The new cheap express method for the 2d-detection of cavities in structure was offered and applied for the preliminary assessment of the molecular slips probability in crystals.
Testing with experimental results showed a good match within the simulated and real properties and transformations for three pharmaceutic compounds: aspirin, piracetam and ibuprofen.