## Slide 1: Bimodal nanoprobes based on cationic quantum dots and Gd3+ chelates prepared by covalent and dative bonds for optical and magnetic resonance imaging
Samantha Dantas Coiadoa*, Gabriela M. Albuquerquea, Izabel G. Souza Sobrinhaa, Giovannia A. L. Pereiraa, Goreti Pereiraa
aFundamental Chemistry Department, Federal University of Pernambuco, Recife, Brazil.
*e-mail:samanthadantasc@hotmail.com
RESULTS
CONCLUSION
INTRODUCTION
METHODOLOGY
Magnetic Resonance Imaging (MRI) is a non-invasive diagnostic technique that allows the visualization of soft tissues. Despite offering advantages over other methods, it has low sensitivity, making it necessary sometimes to use contrast agents (CAs). To improve de CAs efficiency, new strategies have been developed. Among them are the bimodal systems that associate nanoparticles and gadolinium chelates.1
Quantum dots (QDs) are fluorescent nanoparticles, made of semiconductor material, that have unique optical properties. These nanoparticles have been widely used in biomedicine, because they have an active surface, allowing conjugation with (bio)molecules. Thus, they can contain a large number of Gd3+ complexes on their surface, consequently increasing the contrast enhancement.2
In this work, CdTe QDs functionalized with cysteamine were conjugated to gadolinium complexes (DOTA e DTPA), obtaining bimodal systems with optical and paramagnetic properties.
For CdTe-DTPA-Gd systems, it was not observed a significant difference between the two methodologies. However, for the bimodal systems CdTe-DOTA-Gd, the covalent approach seems more adequate, since the relaxometric properties were enhanced, giving CAs with a relaxivity value of 3 times higher thant the clinically used DOTA-Gd. The results obtained showed that these systems are promising bimodal agents for biological studies by fluorescence and MRI.
Systems | T1 (ms) | r1* (mM-1s-1) | 
 |  | Per Gd | Per QD
CdTe-CIS | 3630 | - | -
A1 | 1710 | 7,3 | 29,5
A2 | 1376 | 13,7 | 43,1
C1 | 1750 | 6,2 | 25,1
C2 | 2400 | 3,3 | 10,3
DOTA
NHS
Gd3+
(GdCl3)
EDC
DTPAa
DOTA
NHS
Gd3+
(GdCl3)
EDC
DTPAa
OR
OR
CdTe-DTPA-Gd
(A1 e C1)
CdTe-DOTA-Gd
(A2 e C2)
Optical characterization
Relaxometric characterization
Covalent
System A1: 1) DTPAa + EDC+NHS; 2) QD; 3) Gd3+
System A2: 1) DOTA + EDC+NHS; 2) Gd3+ ; 3) QD
Non-covalent
System C1: 1) DTPAa + EDC+NHS; 2) CIS; 3) Gd3+; 4) QD
System C2: 1) DOTA + EDC+NHS; 2) CIS; 3) Gd3+; 4) QD
CIS
NHS
EDC
Gd3+
(GdCl3)
References:
1Pereira, G. A.; Geraldes, C. F. G. C., Ann Magn Reson 2007, 6, 1-33.
2Pereira, G.; Leite, E. S.; Pereira, G. A. L.; Fontes, A.; Santos, B. S. Quantum Dots. In: Margarita Sanchez-Dominguez, Carlos Rodriguez-Abreu. (Org.). Nanocolloids. 1ed.: Elsevier, 2016, 1, 131-158.
3Matos, A. L. L.; Pereira, G.; Cabral Filho, P. E.; Santos, B. S.; Fontes, A. J. Photochem. Photobiol. B, 2017, 171, 43.
Acknowledgements: CNPq, CAPES and UFPE.
Covalent Approach
Non-Covalent Approach