## Slide 1: Highly Active Pandanus Nanocellulose-supported Poly(amidoxime) Copper (II) Complex for Ullmann Cross-coupling Reaction by: Choong Jian Fui Supervised by:
MAIN SUPERVISOR | PROF. DR. MD LUTFOR RAHMAN
CO-SUPERVISOR | DR. MOHD SANI BIN SARJADI

## Slide 2: Background

## Slide 3
Synthesis process is necessary due to the molecular complexity and various type of bond formation through the organic transformations is being grown in parallel fashion.
C‐C or C-N bonds formation (cross-coupling) reactions are important for the synthesis of essential chemicals such as:
1. Fine chemicals,
2. Drug and intermediate products,
3. Natural products etc.
Transition metal catalysts (Pd, Cu, Ni) are normally used for cross-coupling reactions (suzuki, heck, sonogashira, click etc.).

## Slide 4
Homogeneous catalyst | Heterogeneous catalyst
Expensive | Less expensive
Purification of product is difficult | Easy to purify the product
Can not be reused | Reusable
Environmental pollution | Environmental-friendly
Not stable in the reaction media | Stable under harsh conditions
Catalyst
Homogeneous
Heterogeneous

## Slide 5
Price of the catalyst and catalyst market are growth year by year.
Therefore, the low cost, high activity, high stability, safe reusability, non-toxic, sustainable chemistry, and characteristic of green organic synthesis are well interest by most of the researcher in the development of heterogeneous metal catalyst

## Slide 6: objectives

## Slide 7
To extract the cellulose from the agro-waste (pandanus fruit fibre) and utilize to synthesize a poly(amidoxime) ligand,
To prepare heterogeneous copper catalysts from the cellulose-supported amidoxime ligands,
To evaluate the catalytic ability and reusability of synthesize catalyst in Ullmann cross-coupling reaction.

## Slide 8: Methodology

## Slide 9: Cellulose Extraction
Filter the wood sawdust and weight 100g of fiber.
Dry the cellulose with oven at 50 for one day and weight the mass of cellulose obtain
(Sources: Rahman et al., 2016)

## Slide 10: Synthesize nanocellulose
Procedure:
Boil the cellulose with 40% of H2SO4 for 1 hours.
Pour the mixture into the cool water after reaction done.
Neutralize the solution using NaOH .
Wash and dry.

## Slide 11: Graft Copolymerization (Poly(acrylonitrile))
(Sources: Mandal et al., 2016)
Procedure:
Hydrolyze cellulose react with ceric initiator in inert condition for 15 min
Purified monomer (methyl acrylate) is added.
Heat for 4 hours at 55.
Wash and dry

## Slide 12: Synthesis of Poly(amidoxime) Ligand
(Sources: Shaheen et al., 2016)
Procedure
Hydroxylamine hydrochloride is dissolved into 4:1 methanolic solution.
PMA is added into the hydroxylamine solution and heat for 6 hours at 70.
PHA ligand is washed by methanolic solution.
In order to cover chelating polymeric ligand into H-form ligand, the ligand was treating with 100 mL of 0.1 M of hydrochloric acid (HCl) in methanolic for five minutes.
Wash and dry.

## Slide 13: Preparation Of Metal Catalyst (Cu2+)
Shake for 2 hours with 180 rpm Agitation speed
Wash the ligand and dry it. The ICP-OES analysis should be used to estimate the copper adsorbed
(Sources: Rahman et al., 2016)

## Slide 14: Reaction Mechanism

## Slide 15: Ullmann Reactions
Cu(II)@PAM
base, heat, solvent

## Slide 16: result

## Slide 17: Product
Cellulose from Pandanus fruit fibre
Extraction: 49.5 g from 100g dried fruit fibre
Yeld: (%)
(nanocellulose)
Pandanus fruit and its fibre

## Slide 18: Physical stability of cellulose and nanocellulose
15 min String
Leave For 3 hour
Cellulose
nanocellulose
Cellulose
nanocellulose

## Slide 19: Particle size and zeta potential analysis

## Slide 20: Product
Poly(amidoxime) Ligand
Yield: 28.50g from 10g dried poly(acrylonitrile)
Cu(II)@PAM
ICP-OES= 0.50mmol/g of copper
Poly(acrylonitrile)
Yield: 18.15 g from 10g dried nanocellulose

## Slide 21: FT-IR Analysis

## Slide 22: FE-SEM Analysis
Pandanus fruit fiber
Pandanus-cellulose
Magnification: 1000X

## Slide 23: FE-SEM analysis
nanocellulose
Magnification: 1000X
Poly(acrylonitrile)
Magnification: 5000X

## Slide 24: FE-SEM Analysis
Poly(amidoxime)
Magnification: 5000X
Cu(II)@PAM

## Slide 25: Energy Dispersive X-ray Diffraction (EDX Analysis)
Cu(II)@PAM
Copper = 35.4%
Carbon = 40.7%
Oxygen = 20.2%
Nitrogen= 3.8%

## Slide 26: Tga & DSC

## Slide 27: Xrd RESULT

## Slide 28: XPs Analysis

## Slide 29: Optimization Of Ullmann Reaction

## Slide 30: Reaction

## Slide 33
Mechanism for Ullmann Reaction

## Slide 34: Reusability
Chart: cycle
| 1 | 2 | 3 | 4 | 5 | 6 | 7
Yield(%) | 99 | 97 | 98 | 98 | 99 | 97 | 97

## Slide 35: Leaching Study

## Slide 36: Conclusion

## Slide 37
Successful synthesis high active, stable and safe copper catalyst for Ullmann etherification reaction.
The synthesized copper catalyst can afford the Ullmann etherification in good to high yield of product.

## Slide 38: Future work

## Slide 39
Test the synthesize catalyst in other cross-coupling reaction (C-C, C-N, C-S, etc.)
Utilize the Cu(II)NPs@PAM in total synthesis of natural product, medicine compound.

## Slide 40: References

## Slide 41
D. Meijere A, Diederich F, editors. In Metal-Catalyzed Cross-Coupling Reactions, Second Completely Revised and Enlarged Edition.,
2004, Vol. 2.
Diederich F, Stang PJ, editors. Metal-catalyzed Cross-Coupling Reactions. 1998, Vol.1.
Knochel P, Leuser H, Gong LZ, Perrone S, Kneisel FF. Chem Organozinc Compd. 2006, 287.
Knochel P, Leuser H, Gong L-Z, Perrone S, Kneisel FF. Polyfunctional zinc organometallics for organic synthesis. 2005, 1
Fouquet E, Herve A. Polyfunctional tin organometallics for organic synthesis. 2005, 1
Shimizu M, Hiyama T. Polyfunctional silicon organometallics for organic synthesis. 2005, 1
Knochel P, Krasovskiy A, Sapountzis I. Polyfunctional magnesium organometallics for organic synthesis. 2005, 1
Knochel P, Ila H, Korn TJ, Baron O. Functionalized organoborane derivatives in organic synthesis. 2005, 1
Knochel P, Kopp F. Handbook of functionalized organometallics. 2005, 1
Stephenson GR. Polyfunctional electrophilic multihapto-organometallics for organic synthesis. 2005, 2
Rilatt I, Jackson RFW. J Org Chem. 2008; 73:8694.
Netherton MR, Fu GC. Angew Chem, Int Ed. 2002; 41:3910.
Anderson TJ, Jones GD, Vicic DA. J Am Chem Soc. 2004; 126:8100.
Jones GD, McFarland C, Anderson TJ, Vicic DA. Chem Commun., 2005, 4211.
Fürstner A, Martin R, Krause H, Seidel G, Goddard R, Lehmann CW. J. Am Chem Soc., 2008, 130:8773.
Kleimark J, Hedström A, Larsson P-F, Johansson C, Norrby P O. ChemCatChem. 2009, 1:152.
Md. S. Islama, B. H. Mandalab, T.K. Biswasac, Md. L. Rahman, S. S. Rashida, S.H. Tana and S. M. Sarkar. J. Name., 2012, 3, 1-3
S. L. Xie, Y. H. Hui, X. J. Long, C. C. Wang, Z. F. Xie, Chin. Chem. Lett., 2013, 24, 28.
O. Vassylyev, J.Chen, A.P. Panarello, J.G. Khinast, Tetrahedron Lett., 2005, 46, 6865.
C. Descorme, P. Gallezot,C. Geantet, and C. George. Chem. Cat. Chem., 2004, 1, 1 – 11.
K.K.R. Datta, M. Eswaramoorthy, C.N.R. Rao, J. Mater. Chem. 2007, 17, 613.
J. Zhu, J. Zhou, T. Zhao, X. Zhou, D. Chen, W. Yuan, Appli. Catal. A: Gen., 2009, 352,

## Slide 42
S.J. Guo, J. Bai, H.O. Liang, C.P. Li, Chin. Chem. Lett. 2016, 27, 459–463.
M.J.G. Escalonilla, P. Atienzar, J.L.G. Fierro, H. Garcıa, F.J. Langa, Mater. Chem., 2008, 18, 1592–1600.
J.G. de Vries, Can. J. Chem., 2001, 79, 1086–1092.
S.S. Shendage, U.B. Patil, J.M. Nagarkar, Tetrahedron Lett., 2013, 54, 3457.
L.F. García, M. Blanco, C. Blanco, P. Álvarez, M. Granda, R. Santamaría, R.J. Menéndez, Mol. Catal. A: Chem., 2016, 416, 140–146.
C. Shen, H. Shen, M. Yang, C. Xia, P. Zhang, Green Chem., 2015, 17, 225–230.
P. Cotugno, M. Casiello, A. Nacci, P. Mastrorilli, M.M. Dell’Anna, A. Monopoli, J.
Organomet. Chem., 2014, 752, 1–5.
J. Li, X.Y. Shi, Y.Y. Bi, J.F. Wei, Z.G. Chen, ACS Catal., 2011, 1, 657.
P. Nehra, B. Khungar, K. Pericherla, S.C. Sivasubramanian, A. Kumar, Green Chem., 2014, 16, 4266–4271.
M.S. Sarkar, H. Qiu, M.J. Jin, J. Nanosci. Nanotechnol., 2007, 7, 3880–3883.
L. Jin, J. Liebscher, Chem. Rev., 2007, 107, 133
M. L. Rahman, S. M. Sarkar, M. M. Yusoff, M. H. Abdullah. RSC Adv., 2016, 6, 745-757.
M. L. Rahman, S. M. Sarkar, M. M. Yusoff. Front. Environ.l Sci. Eng., 2016, 10, 352-361.
S. M. Sarkar, T. Sultana, T. K. Biswas, M. R. Lutfor, M. M. Yusoff, New J. Chem. 2016, 40, 497.
O. A. Anunziata, M. L. Martínez and A. R. Beltramone. Materials, 2009, 2(4), 1508-1519.
Y. Han, G. Hwanga, H. Kima, B.Z. Haznedaroglu, B. Lee, Chem. Eng. J. 2015, 259, 653.
M. S. Sarkar, M. R. Lutfor, M. M. Yusoff, RSC Adv. 2015, 5, 1295.
D. Zhao, J. Feng, G. D. Stucky, Science, 1998, 279, 548.
T. F. Parangi, R. M. Patel and U. V. Chudasama. Bull. Mater. Sci., 2014, Vol. 37, No. 3, 609–615.
B. H. Mandal, M. R. Lutfor, M. M. Yusoff, K. F. Chong, S. M. Sarkar, Carbohydrate Polym. 2017, 56, 175.
S. M. Sarkar, Md. L. Rahman, and M. M. Yusoff. RSC Adv., 2014, 00, 1-3.
B. Yuan, Y. Pan, Y. W. Li,* B. Yin, and H. F. Jiang. Angew. Chem. Int. Ed., 2010, 49, 4054 –4058