## Slide 1
Mapping of novel binary copper oxides with
density functional theory modelling
S. Sampath1, K. Tokar1,2, M. Derzsi1,3
1Advanced Technologies Research Institute, Faculty of Materials Science and Technology in Trnava,
Slovak University of Technology in Bratislava, Jána Bottu 8857/25, 917 24 Trnava, Slovakia
2Institute of Physics, Slovak Academy of Sciences, Dúbravská cesta 9, 845 11 Bratislava, Slovakia
3Center of New Technologies, University of Warsaw, Żwirki i Wigury 93, 02089 Warsaw, Poland
sankari.sampath@stuba.sk
10-20 November

## Slide 2: Introduction
Binary copper oxides [Cu-O] have remarkable electronic and optical properties.
Cu-O find numerous applications in photovoltaics and all-oxide electronics due to their abundance, low cost and non-toxic nature that makes Cu-O highly attractive for further exploration.
Our Goal - To predict new stable binary Cu-O phases using density functional theory (DFT) and Evolutionary Algorithm (EA) methods.

## Slide 3: Known binary Cu-O
[1] Benxian L et.al, J. Solid State Chem., 184, 2097 (2011)
[2] Chaudhary N et.al, Solid State Commun., 247, 36 (2016)
[3] Morgan P E D et.al, J. Solid State Chem., 121, 33 (1996)
CuIIO[2]
Tenorite
CuI2CuII2O3[3]
Paramelaconite
C2/c
a = 4.691Å, b = 3.417Å,
c = 5.13Å, β = 99°
I 41/ a m d
a = b = 5.818Å,
c = 9.894Å
CuI2O[1]
Cuprite
P n -3 m
a = 4.271Å

## Slide 4: Computational procedure
Input models (Lit.,)
DFT optimisation
Spin polarised calculation DFT+U
High- and low-spin solutions (HS/LS)
Lattice dynamics
Evolutionary
algorithms
Databases

## Slide 5: Calculation details
DFT method for structure optimization (VASP program).
Details of the DFT calculations: PBEsol functional, planewave cut-off 520eV.
Electron correlations handled with Liechtenstein approach: UCu=9eV, JCu=1eV.
EA for the search of crystal structures (XtalOpt program[4]).
Lattice dynamics calculations using program PHONOPY[5].
[4] Patrick A et.al, Comput. Phys. Commun., 222, 418 (2018)
[5] Togo A et.al, Scr. Mater., 108, 1 (2015)

## Slide 6: Strategy for the selection of input models

## Slide 7: Cu3O2 Stoichiometry
NaCu2O2 Structural type
P n m a
a = 5.896Å, b = 2.827Å, c = 2.139Å

## Slide 8: Cu3O4 Stoichiometry
Calculated both HS and LS solutions. Only LS solution is stable.
Ag3O4 Structural type
P 1 21 / c 1
a = 3.298Å, b = 8.454Å,
c = 5.005Å, β = 102.9°

## Slide 9: Cu2O3 Stoichiometry
Superoxide(EA) Structural type
P 1
a = 2.789Å, b = 5.957Å,
c = 6.578Å, α = 93°; β = 102.9°; γ = 94°
Compound (spin) | a (Å) | b (Å) | c (Å) | V/Z (Å)3 | ΔE/Z (eV) | Mag. (mB)
Superoxide(EA) (FM) | 2.794 | 5.927 | 6.582 | 50.661 | 0.006 | 0.626
Superoxide(EA) (AFM) | 2.789 | 5.957 | 6.578 | 50.886 | 0.000 | +0.627 -0.581
O-O bridge

## Slide 10: Impact of lattice dynamics on the stability of the models
Na2CuO2 structure type
Ag3O4 structure type
Phonon dispersion curves
Cu3O2
Cu3O4

## Slide 11: Convex Hull
Thermodynamically, Convex Hull represents the enthalpy.
Correctly predicted the stability of existing phases.
3 new Cu-O phases are stable with respect to elements Cu, O and Cu2O phase.
Cu3O4 and Cu2O3 are stable with respect to Cu4O3.
3 new phases are metastable in respect to CuO phase.
Cu3O2 = -0.578eV/atom,
Cu3O2 = -0.551eV/atom
Cu3O2 = -0.515eV/atom.

## Slide 12: Conclusions
Crystal structures of 3 new Cu-O compounds are predicted – Cu3O2, Cu3O4 and Cu2O3.
Cu3O2 was predicted for Na2CuO2 type structure.
Cu3O4 was predicted as a low spin Ag3O4 structural type.
Cu2O3 was predicted as a AFM superoxide (EA) type.
The new structure types found to be dynamically stable.
Correctly predicted the stability of existing binary Cu-O phases.
The newly predicted Cu-O phases are stable with respect to elements Cu, O and Cu2O phase.
Cu3O4 and Cu2O3 are stable with respect to Cu4O3.

## Slide 13: Acknowledgements
The European Regional Development Fund, Research and Innovation Operational Programme, for project No. ITMS2014+: 313011W085.
Scientific Grant Agency of the Slovak Republic, grant No. VG 1/0223/19.
The Slovak Research and Development Agency, grant No. APVV-18-0168.
Aurel supercomputing infrastructure in CC of Slovak Academy of Sciences acquired in projects ITMS 26230120002 and 26210120002 funded by ERDF.

## Slide 14
Thank you for your attention!