## Slide 1
jsimal@uvigo.es juste@uvigo.es
Multiple SERS detection of phenol derivatives in tap water
A. Carreira-Casais1,V. Montes-García2 , I. Pastoriza-Santos2, M. Prieto1, J. Simal-Gándara1 J. Pérez-Juste2
1Nutrition and Bromatology Group, Department of Analytical and Food Chemistry, Faculty of Science, University of Vigo, Vigo, Spain.
2Department of Physical Chemistry, Biomedic Research Center of Galicia (CINBIO) University of Vigo, Vigo, Spain.

## Slide 2: INDEX
Introduction
  Why phenols are important?
  Phenols detection
  Why we had employed SERS?
Aim
Results
Conclusion

## Slide 3: INTRODUCTION
WHY ARE PHENOL DERIVATIVES IMPORTANT FOR US?
a) Some phenol derivatives are employed as pesticides or are metabolites of pollutants.
b) They are produced by oil industry and are widely distributed in soils and water.
c) Many of them are really noxious for human health.

## Slide 4: INTRODUCTION

## Slide 5: INTRODUCTION
PHENOLS DETECTION
We prove a method to demonstrate that we are able to detect PHENOL, O-CRESOL AND 1-NAPHTHOL in tap water using Surface-enhanced Raman spectroscopy (SERS).

## Slide 6: INTRODUCTION
WHY WE HAD EMPLOY SERS?
SERS is a really powerful method that allow us to detect pollutants without a great preparation of the sample.
Zhao et al., Front. Microbiol, 2018

## Slide 7: INTRODUCTION
The method is based on the colorimetric reaction between a phenol and the indophenol (Gibbs reactive) to form and indophenolate. Our aim is to determitate phenols simultaneously
Colorless
Green-colored product
Conditions: t: 2500 s ; Gibss Reagent Concentration (DBQC) 5X10-5 M
UV-VIS

## Slide 8: RESULTS Plasmonic Substrates
Plasmonic substrates were made with 60 nm Au@Nps

## Slide 9: RESULTS Phenol calibration
Each spectra and point is the average of 16 single spectra
dbqc
phenol 0.25 µM
phenol 1 µM
phenol 5 µM
Fitted using a Hill-Langmuir equation y = A1 x (exp) (-x/t1) +y0

## Slide 10: RESULTS First Step for Multiplex detection
WE COMPARE 3 SAMPLES AT THE SAME CONCENTRATION
phenol 5 µM
1-naphthol 5 µM
o-cresol 5 µM

## Slide 11: RESULTS First Step for Multiplex detection
WE COMPARE 3 SAMPLES AT THE SAME CONCENTRATION
phenol 5 µM
1-naphthol 5 µM
o-cresol 5 µM

## Slide 12: RESULTS Semiquantitative detection
1-naphthol/o-cresol Binary Mixture
and
1-naphthol 5 µM
o-cresol 5 µM
Binary Mixture 1:1 5 µM
Semi-quantitative detection performed as Zou, S. et al., Sci. Rep. 2017, 7.

## Slide 13: RESULTS Semiquantitative detection
1-naphthol/o-cresol Binary Mixture
and
Semi-quantitative detection performed as Zou, S. et al., Sci. Rep. 2017, 7.

## Slide 14: RESULTS Semiquantitative detection
phenol / 1-naphthol Binary Mixture
and
phenol 5 µM
1-naphthol 5 µM
Binary mixture 1:1 5 µM

## Slide 15: RESULTS Semiquantitative detection
phenol / 1-naphthol Binary Mixture
and

## Slide 16: RESULTS Semiquantitative detection
phenol/ o-cresol Binary Mixture
and
phenol 5 µM
o-cresol 5 µm
Binary mixture 1:1 5 µM

## Slide 17: RESULTS Semiquantitative detection
phenol/ o-cresol Binary Mixture
and

## Slide 18: CONCLUSIONS
1) This method allow to quantify the amount of this 3 phenol derivatives, and to differenciate between them.
2) This method allow to perform a semi-quantitative determination of binary mixtures.
3) We purpose that this experiment could be a new step in the rapid-screening of contamination in water.
On going work:
-Semiquantitative detection of ternary mixtures.

## Slide 19: ACKNOWLEDGEMENTS
Anxo Carreira-Casais thanks the Ministerio de CIencia, Innovación y Universidades for his FPU 16/06135 fellowship.