## Slide 1
Title of the Presentation
Junwei Xu 1,2, Ping Li 1,2 ,*, and Yubo Fan 2,3 ,*
1 School of Biological Science and Medical Engineering, BUAA, Beijing, China;
2 Beijing Advanced Innovation Centre for Biomedical Engineering, BUAA, Beijing, China;
3 School of Medical Science and Engineering, BUAA, Beijing, China.
* Corresponding author: liping@buaa.edu.cn; yubofan@buaa.edu.cn
Preparation of Magnetic-Fluorescent Bifunctional Microrods as a Drug Delivery System via One-step Electrospraying

## Slide 2
Abstract:
☞ Magnetic-fluorescent bifunctional drug delivery system which possesses magnetic targeting and fluorescent tracing capabilities, effectively improves the delivery efficiency of drugs.
☞ With the in-depth study of the properties of non-spherical microparticles, it is found that the shape of the microparticles also plays a key role in drug delivery.
☞ Because of the unique shape, rod-like microparticles have exhibited great drug molecule metabolic dynamics and excellent anti-tumor effects during the process of treatment.
☞ In this study, Fe3O4/NaYF4:Eu3+/PLGA magnetic- fluorescent bifunctional microrods were prepared via one-step electrospraying.
Keywords:
♢ One-step electrospraying; ♢ Microrods;
♢ Drug delivery system; ♢ A549 cells；
♢ Magnetic-fluorescent bifunctional

## Slide 3
1. Background
2. Materials & Methods
3. Results & Discussion
4. Conclusions
Content

## Slide 4
Background
Drug delivery system
Magnetic-fluorescent
Shape influence

## Slide 5
Drug delivery system
Chen H.B., et al. Sci. China Chem. 2018,61:1503
In order to improve the efficiency of drug utilization, drug delivery system (DDS) was proposed and used for delivering and then releasing the drugs to the lesion as well as reducing the toxicity of drugs.
Yu X.F., et al. Angew. Chem. Int. Edit. 2020, 59: 20568

## Slide 6
Zhang M., et al. PNAS, 2018,115:6590
Magnetic-fluorescent
With magnetic targeting and fluorescent labeling functions, the DDS could realize the integration of diagnosis and treatment such as biological imaging and drug delivery.
With the development of DDS, researchers paid more attention to the delivery targeting efficiency of DDS, especially that with magnetic targeting and fluorescence tracer.
Mandal K., et al. Appl. Nano Mater. 2019, 2, 3292

## Slide 7
Lu Y., et al. Adv. Mater., 2001,13:271
Zhang H., et al. J Control. Release, 2016,244:52
Shape influence
The regulation in the morphology, size, and surface composition of the carrier also affects the therapeutic effect of the DDS.
With the large specific surface area, high drug-loading capacity, long circulation time and high cell uptake efficiency, the rod-shaped DDS has a better effect than the spherical DDS in the
treatment of cancer and other diseases

## Slide 8
Materials
& Methods
Preparation
Characterization

## Slide 9
Materials & Methods
Figure 1. Schematic illustration of the preparation of the Fe3O4/NaYF4:Eu3+/PLGA magnetic-fluorescent bifunctional microrods.

## Slide 10
Characterization
Fe3O4/NaYF4:Eu3+/
PLGA microrods
SEM: Morphology
Infrared analysis
Thermal stabilities
Magnetic property
Fluorescent property
Fe3O4/NaYF4:Eu3+/
PLGA microspheres
Hydrophobicity
Cytotoxicity
DOX-loaded
Entrapment efficiency
Drug-loading capacity
Anti-cancer cell efficiency

## Slide 11
Results
& Discussion
Morphology
Composition
Magnetic property
Fluorescent property
Hydrophobicity
Cytotoxicity
Drug loading capacity
Anti-cancer cell efficiency

## Slide 12
Figure 2. SEM images of Fe3O4/NaYF4: Eu3+/PLGA microrods at different magnifications, (a) ×5000, (b) ×10000; (c) length distribution and
(d) diameter distribution of Fe3O4/NaYF4: Eu3+/PLGA microrods.
Morphology
Fe3O4/NaYF4: Eu3+/PLGA microrod possessed uniform rod shape.

## Slide 13
Figure 3. (a) FTIR spectra of PLGA and Fe3O4/NaYF4:Eu3+/PLGA microrods; (b) TG curve of PLGA and Fe3O4/NaYF4: Eu3+/PLGA microrods.
Composition
Infrared analysis and thermal stabilities

## Slide 14
Figure 4. Hysteresis loop of (a) pure Fe3O4 MNPs and (b) Fe3O4/NaYF4:Eu3+/PLGA microrods. (c) Optical microscope images of Fe3O4/NaYF4:Eu3+/PLGA microrods.
The saturation magnetizations of the pure Fe3O4 MNPs and Fe3O4/NaYF4:Eu3+/PLGA microrods were 67.4 and 4.6 emu/g, respectively.
Fe3O4/NaYF4:Eu3+/PLGA microrods still exhibited great magnetic properties.
Magnetic property

## Slide 15
Figure 4. Emission spectra of (d) pure NaYF4:Eu3+ NPs and (e) Fe3O4/NaYF4:Eu3+/PLGA microrods. (f) Fluorescent photograph of the Fe3O4/NaYF4:Eu3+/PLGA microrods.
Fluorescent property
The intensity of emission spectra and the fluorescence photograph suggested the excellent luminescent property of Fe3O4/NaYF4:Eu3+/PLGA microrods which would be a good candidate for bioimaging and drug tracer.

## Slide 16
Figure 5. Images of water droplets on (a) Fe3O4/NaYF4:Eu3+/PLGA microrods and (b) Fe3O4/NaYF4:Eu3+/PLGA microspheres; (c) contact angles and of Fe3O4/NaYF4:Eu3+/PLGA microrods and microspheres, n=3.
Hydrophobicity
The microrods exhibited a smaller contact angle of approximately 9.7 °than the microspheres, which suggested that microrods were more hydrophilic than microspheres.

## Slide 17
Figure 6. (a) Fluorescence images of HUVECs and A549 cells (stained with AO) cultured with microrods or microspheres at the concentration of 1 mg/mL for 5 d, scale bar: 100 μm. In vitro cell relative viabilities of (b) HUVECs and (c) A549 cells co-cultured with Fe3O4/NaYF4:Eu3+/PLGA microrods or microspheres at the concentration of 1 mg/mL for 1 d, 3 d and 5 d, n=3.
Cytotoxicity
No significant cytotoxicity to HUVECs and A549 cells !

## Slide 18
Figure 7. The calculated EE and LC of DOX loaded Fe3O4/NaYF4:Eu3+/PLGA microrods and microspheres, n=3.
Drug loading capacity
The entrapment efficiency and drug-loading capacity of DOX loaded Fe3O4/NaYF4:Eu3+/PLGA microrods were 9.153±0.506% and 0.907±0.050%, higher than 8.368±0.259% and 0.830±0.025% of DOX loaded Fe3O4/NaYF4:Eu3+/PLGA microspheres.
The high drug loading capacity might due to the larger specific surface area in comparasion with microspheres.

## Slide 19
Figure 8. (a) In vitro A549 cell relative viabilities normalized to the untreated control after co-cultured with DOX loaded Fe3O4/NaYF4:Eu3+/PLGA microrods or microspheres at different concentrations of 0.1, 0.2, 0.5, 1.0, 2.0 or 5.0 mg/mL for 48 h, n=3. (C) In vitro A549 cell relative viabilities normalized to the untreated control at the concentration of 1.0 mg/mL for 12, 24, 48 and 72 h, n=3.
Anti-cancer cell efficiency
The drug-loading Fe3O4/NaYF4:Eu3+/PLGA microrods had stronger killing effects to cancer cells in comparison with microsheres.

## Slide 20
Conclusions
Conclusions
Acknowledgments

## Slide 21
Conclusions
☺ The Fe3O4/NaYF4:Eu3+/PLGA microrods showed a good rod.
☺ The microrods had outstanding magnetic and fluorescent properties.
☺ Compared with microspheres, microrods had better hydrophilic property.
☺ there was no obvious cytotoxicity of Fe3O4/NaYF4:Eu3+/PLGA microrods.
☺ Microrods had a higher entrapment efficiency and drug-loading.
☺ Compared with microspheres, microrods had stronger killing effects to cancer cells (after loading DOX).
In short, this rod-shaped drug carrier, Fe3O4/NaYF4:Eu3+/PLGA microrods, with magnetic-fluorescent bifunctional have a good prospect in the field of drug delivery.

## Slide 22
Acknowledgments
This study was supported by funds from National Natural Science Foundation of China (NSFC) Research Grants (61871014, 52071008, 11827803, 11421202), and it was also supported by Beijing Natural Science Foundation (7191006).
Prof. Y.B. Fan
Beijing Advanced Innovation Centre for Biomedical Engineering
Beihang University
Beijing 100191, P. R. China
E-mail: yubofan@buaa.edu.cn
Prof. P. Li
School of Biological Science and Medical Engineering
Beihang University
Beijing 100191, P. R. China
E-mail: liping@buaa.edu.cn

## Slide 23
Our group~

## Slide 24
Thanks!