## Slide 1
Design, preparation and characterization of lactoferrin-loaded sulfobutylether-β-cyclodextrin/chitosan nanoparticles as a therapeutic alternative for keratoconus treatment
R. Varela-Fernández1,2, X. García-Otero1, M. I. Lema-Gesto2, M. González-Barcia3, and F. J. Otero-Espinar1
Department of Pharmacology, Pharmacy and Pharmaceutical Technology. University of Santiago de Compostela (USC). Campus vida. Santiago de Compostela. Zip Code: 15782. Spain. francisco.otero@usc.es.
Clinical Neurosciences Group. University Clinical Hospital, Health Research Institute of Santiago de Compostela (IDIS). Travesía da Choupana s/n Santiago de Compostela. Zip Code: 15706. Spain. mariaisabel.lema@usc.es.
Molecular Imaging Group. University Clinical Hospital, Health Research Institute of Santiago de Compostela (IDIS). Travesía da Choupana s/n Santiago de Compostela. Zip Code: 15706. Spain.
Clinical Pharmacology Group. University Clinical Hospital, Health Research Institute of Santiago de Compostela (IDIS). Travesía da Choupana s/n Santiago de Compostela. Zip Code: 15706. Spain. miguel.gonzalez.barcia@sergas.es.
Introduction and objectives
Lactoferrin has shown potential as a good therapeutic alternative in the treatment of Keratoconus [1]. Chitosan/Cyclodextrin nanoparticles as novel drug delivery systems (DDS) could successfully encapsulate hydrophobic drugs [2]. The aim of this work was based on the design, preparation, and characterization of lactoferrin-loaded CS/SBE-β-CD nanoparticles as topical ophthalmic DDS for the keratoconus treatment.
Methodology
Results
Preparation of lactoferrin CS/SBE-β-CD NPs
Characterisation of lactoferrin CS/SBE-β-CD NPs
Lactoferrin
SBE-β-CD
Topical ophthalmic administration
Lactoferrin/SBE-β-CD inclusion complexes
Chitosan
Chitosan
Phase diagram of nanoparticle's formation and physicochemical characterization
Sample preparation
Freeze-drying
Production yield (PY)
Encapsulation efficiency (EE)
Loading capacity (LC)
Imaging analysis
SEM and TEM analysis
Size and  Potential
Nanoparticles were spontaneously obtained via ionotropic gelation. 1 ml lactoferrin/SBE-β-CD aqueous solution was added to 3 ml CS acidic aqueous solution under magnetic stirring at room temperature.
Phase diagram reveals that only CS/SBE-β-CD specific ratios lead to nanoparticle’s formation. The appearance of opalescence was used as an indicator of nanoparticle formation, also confirmed by Dynamic Light Scattering (DLS).
Low amounts of initial CS/SBE-β-CD give rise to no nanoparticle’s formation, while precipitation occurred when high amounts of initial compounds were used.
Long-term stability to storage study
Phase diagram formation for lactoferrin-loaded CS/SBE-β-CD nanoparticle’s formation.
Morphological characterisation of nanoparticles
Conclusion
Lactoferrin-loaded CS/SBE-β-CD nanoparticles were proposed as a new ocular drug delivery system with the virtue of easy administration, prolonged drug release time, improved ocular bioavailability and reduced dosing frequency. Lactoferrin CS/SBE-β-CD nanoparticles show considerable potential as hydrophilic drug carrier and have the capacity to deliver drugs to specific target sites, possibly revolutionizing the Keratoconus therapy.
Bibliography
[1] Mas Tur V, MacGregor C, Jayaswal R, O’Brart D, Maycock N. A review of keratoconus: Diagnosis, pathophysiology, and genetics. Surv Ophthalmol. 2017 Dec;62(6):770–83.
[2] Jingou J, Shilei H, Weiqi L, Danjun W, Tengfei W, Yi X. Preparation, characterization of hydrophilic and hydrophobic drug in combine loaded chitosan/cyclodextrin nanoparticles and in vitro release study. Colloids Surf B Biointerfaces. 2011;83(1):103-7.
Scanning electron micrographs show that lactoferrin-loaded CS/SBE-β-CD nanoparticles were predominantly spherical in shape.
Transmission electron microscopy images indicate that these nanosystems may have an irregular surface.
Scanning Electron Microscopy (SEM)
Transmission Electron Microscopy (TEM)
Changes in size and PDI values during the optimization procedure of CS/SBE-β-CD nanoparticles.