## Slide 1
Protein mixture
Sustained GDNF delivery via PLGA nanoparticles
Pablo Vicente Torres-Ortega1,2, Cristian Smerdou 2,3, Elisa Garbayo1,2, María J. Blanco Prieto1,2*
INTRODUCTION
RESULTS
Glial cell line-derived neurotrophic factor (GDNF) is a protein with remarkable trophic actions on dopaminergic neurons which is under investigation for Parkinson's disease (PD) therapy1,2. It is a highly glycosylated biopharmaceutical in which the composition of attached glycans potentially influences drug efficacy and immunogenicity2. Hence, the use of recombinant GDNF from mammalian cells is essential to avoid safety issues2. Moreover, although several approaches to deliver this protein to the brain have been described3, a promising strategy would be the use of nanoparticles (NPs) containing GDNF in the dopamine-depleted brain areas.
The objective of this work is to develop and characterize biodegradable NPs loaded with recombinant GDNF produced in mammalian cells for brain tissue engineering.
Fast Flow
resin
GDNF
Concentration
Electroporation
Centrifugation and filtration
WB analysis
BHK-21 cells
POLYMERIC GDNF-NPs FORMULATION (W1/O/W2)
W1 : hGDNF +Albumin +PEG + PBS
O: PLGA + Organic solvent
W2 : Poly(vinyl alcohol) 1%
hGDNF-loaded NPs preparation and characterization
B) hGDNF purification
A) hGDNF expression in BHK cells
Coomassie Blue staining showed that hGDNF obtained was highly pure
1 Department of Pharmaceutical Technology and Chemistry, Faculty of Pharmacy and Nutrition, Universidad de Navarra, C/ Irunlarrea 1, 31008 Pamplona, Spain
2 Navarra Institute for Health Research, IdiSNA, C/ Irunlarrea 3, 31008 Pamplona, Spain
3 Division of Gene Therapy, School of Medicine, Center for Applied Medical Research (CIMA), University of Navarra, Av. Pío XII 55, 31008 Pamplona, Spain
hGDNF expression and purification
hGDNF-NPs were formulated by double emulsión solvent evaporation using One Recirculation Machine (TROMS) Technology
PC12 cell-based bioassay showed that GDNF remains bioactive after its nanoencapsulation.
Scheme of TROMS Technology
Spherical particles.
Uniform size distribution of NPs.
No aggregation.
In vitro release study of GDNF from NPs
PLGA | MEAN SIZE | PDI | EE%
NPs (n=3) | 405.5 ± 2.9 nm | 0.08 ± 0.03 | 61.65±7
B) NPs characterization
A) hGDNF-loaded NPs preparation
CONCLUSIONS
ACKNOWLEDGEMENTS
GDNF-loaded NPs were successfully prepared by W1/O/W2 emulsion/extraction process using TROMS technology with a high drug entrapment efficiency.
The developed nanosystem has great potential for brain tissue engineering applications.
1. E. Garbayo et al, Effective GDNF brain delivery using microspheres-A promising strategy for Parkinson’s disease.
2. R.A. Barker et al, GDNF and Parkinson’s Disease: Where Next? A Summary from a Recent Workshop.
3. P.V. Torres-Ortega et al, Micro- and nanotechnology approaches to improve Parkinson’s disease therapy.
4. E. Ansorena et al. A simple and efficient method for the production of human glycosylated glial cell line-derived neurotrophic factor using a Semliki Forest virus expression system.
This work was supported by the Spanish Ministry of Education (program FPU (FPU17/01212)) and Government of Navarra (2019_66_NAB9).
E. Garbayo is supported by a “Ramon y Cajal Fellowship (RYC2018-025897-I).
Future perspectives
B1
B3
B2
B4
A two-component hydrogel based on HA functionalization with adamantane (guest) and β-cyclodextrin (host) will be prepared and characterized.
GDNF-NPs will be included in the hydrogel for its local brain administration.
GDNF released within the first 24 hours was 19.10 ± 3.5%, followed by a phase of sustained-release with 50.6 ± 3.1% of GDNF being released within 28 days.
Cation exchange chromatography
REFERENCES
Bioactivity
SEM analysis
Size, PDI and EE