Article

Corrosivity of Hydrocarbon Flows in Oil Pipelines Faysal Fayez Eliyan1,*, Afnan Eliyan2

1	Faysal.Eliyan@ccq.edu.qa

2	aeliyan@qu.edu.qa

*	Correspondence: Faysal.Eliyan@ccq.edu.qa; Tel.: +974-50262050

Abstract: This paper compiles aspects on the corrosivity of hydrocarbon fluids in oil pipelines.  Oil pipelines carry complex mixtures of hydrocarbons, water, gases, and miscellaneous chemicals that, in relation to the physico-chemical and flow conditions, drive internal corrosion in a variety of ways. The paper highlights the water-oil emulsions and multiphase flow regimes, wettability of metal surface, corrosivity of aqueous phase in crude oil, composition of the aqueous phases in hydrocarbon fluids, roles of O2, CO2, sulfur and H2S in the hydrocarbon fluids, and influence of oil chemistry on the corrosivity of the aqueous phase.

Keywords: oil; pipeline; CO2; hydrocarbon; multiphase

- Corrosivity of hydrocarbon fluids

Crude oils are composed of different hydrocarbons, in groups of paraffin, naphthene, and aromatics. The amounts of hydrocarbons in crude oils varies in a wide range depending on the origin of oil. Petroleum products in pipelines are more homogenous in composition than crude oils and contain naphtha with carbon number from C5 to C16 [1]. Corrosivity of crude oils and petroleum products depend on the chemical composition and physical characteristics. Crude oils from deep wells could be as high in temperature as 200oC, but through production units crude oils cool down significantly. Oil transmission pipelines operate below 65oC, at which hydrocarbons are poor electrolytes and non-corrosive. Petroleum products do not contain water, posing no significant corrosion risks for metallic pipes and components handling them. Crude oils, however, could contain significant amounts of water, coexisting with oil, such as those extracted from oil-sand fields in Alberta, Canada, or injected into oil wells to enhance production, or entering pipelines during operational upset. Water and oil are immiscible and form emulsions of different types. Water could exist as dispersed droplets in oil phase or as more continuous entities as a phase. The water phase containing dissolved salts and gases constitute a corrosive medium that could cause different forms of pipeline corrosion. The corrosivity of oils containing water is determined by three factors: type of emulsion of oil and water, wettability of metal surface, and corrosivity of water phase [2]. The prediction of corrosivity of oil-water mixture is shown in Figure 1.

2. Water-oil emulsion and multiphase flow regime

Water and oil are immiscible and they form different flow patterns (flow regimes) during pipeline transportation. A flow pattern depends on oil-to-water ratio, velocity of each phase, viscosity of oil, and geometrical factors, such as the pipe inclination angle [3-8]. At low mixture velocities, the flow takes stratified patterns in which the less dense phase, oil, flows above the denser phase, constituted of water [3]. At high mixture velocities, the flow takes dispersed patterns in which one phase is dispersed within the continuum of the other phase [9]. At intermediate mixture velocities, a combination of the two patterns above appear and the fluids maintain continuity, but with a degree of dispersion, into the continuum of the other [9]. Generally, when water is the continuous phase, the flow pattern does not depend much on oil viscosity, and when oil is the continuous phase, the oil-annulus annular flow, for example, decreased in size in correlation to decreasing oil viscosity.

Figure 1. Predicting influence of crude oil on the corrosivity of the aqueous phase [2].

Figure 2 shows typical flow patterns when oil of viscosity of 84 centipoise at 20 oC intermixes with water in a horizontal pipe. The figure shows a variety of flow patterns, including “stratified”, “mixed”, “annular”, “intermittent” and “dispersed”. Figure 3 shows typical flow patterns of oil-water mixtures flowing in a vertical pipe. The two phases disperse into each other and no stratified flow patterns form.

Transition from one flow pattern to another is an important aspect to consider for pipeline design and corrosion protection – especially that water is the corrosive phase whose distribution and dispersion determines the nature and rate of a corrosion attack. In addition, efficacy of corrosion inhibitors in controlling corrosion rates is influenced by pipeline flow patterns. Mapping flow patterns helps understand and control corrosion better in oil production and transmission pipes in reference to percentage of water and velocity of flow mixture. Figure 4 shows an example of a flow pattern map, for oil of viscosity of 84 centipoise at 20oC [10]. The solid lines represent the changes in flow patterns observed from experiments and dashed lines represent the changes in flow patterns predicted from theory. Stratified flows of complete separation of phases occur at relatively low flow rates over a limited range, under the influence of mainly density and gravity.

Figure 2. Oil–water flow patterns in horizontal pipes [3].

Figure 3. Characterization of oil–water flow patterns in vertical pipes [3].

At high flow rates, the interface becomes wavy with entrainment of water droplets in oil layer or oil droplets entrained in water layer (MO and MW). Gravitational forces influence the interface more than the dynamic forces and the entrained droplets remain near the interface. At low water fractions, water could be entrained in the continuous oil phase, as an annular pattern of water core surrounded by a continuous oil phase (AO). The water-annulus annular flow (AW) is not in the pattern map, as this pattern does not appear with low-viscosity, low-density oils. At higher flow rates, the interface between oil and water loses stability due to the relative movement of phases and formation of vortices in the oil layer penetrating the water layer and vice versa. This turbulence at the interface eventually disperses the flow and the low fraction phase loses its continuity and becomes dispersed in the high fraction phase (DO and DW). The vertical solid lines in Figure 4 represent the reversion of the continuous phase in the flow patterns. Phase inversion, described in Figure 5, occurs at a point defined as a critical volume fraction of the dispersed phase above which it becomes the continuous phase [4, 10, 11]. The critical volume fraction is dependent on oil viscosity and system parameters, including operational conditions, geometry, and pipe materials [12, 13].

Figure 4. Oil–water flow pattern map. S, stratified flow; MO, MW, mixed flow; AO, oil–annulus annular flow; DO, DW, dispersed water in oil and dispersed oil in water [10].

Figure 5. Inversion process for oil–water dispersion flow [10].

It was found that the water fraction required to invert a dispersion decreases with higher oil viscosity, according to the empirical correlation [14]:

(1)

For highly viscous oils (above 0.2 Pas) the critical water cut volume fraction could be nearly 0.15 [14]. Another empirical correlation based on the momentum equations for stratified flows, with negligible interfacial shear and no-slip between the two layers, is proposed as [15]:

(2)

k1 reflects wall/liquids contact perimeter, and k2 accounts for the flow regime in each of transported phases. Breakage forces are due to turbulent and viscous shear in the flow. For stable liquid dispersion, dynamic equilibrium between the two competing drops breakage and drop coalescence maintains.

3. Wettability of metal surface

Corrosion initiates when pipe surface gets in contact with the water phase in the oil-water mixture, in ways depending on the flow patterns and wettability of pipe surface. The tendency of water to displace hydrocarbon from pipe surface is determined from the contact angle of three phase system, and there are three scenarios of surface wettability, shown in Figure 6.

Figure 6. Contact angle measurements through water phase: (a) water wet surface, (b) mixed-wet surface, (c) oil-wet surface.

In Figure 6, θ is contact angle, γos is surface tension of oil-steel interface, γow is surface tension of oil-water interface, and γws is surface tension of water-steel interface. If the surface is unwettable by water, water minimizes its contact with the solid and the contact angle is approximately zero, which is an extreme case, in Figure 6a. If the surface is neither totally water-wetting nor totally oil-wetting the contact angle is between 0 and 180o, in Figure 6b, and the total surface free energy of the three phases is at minimum level. If the surface is wettable with water, water spreads over entire surface and the contact angle is approximately 180o, which is an extreme case.

The contact angle is maintained by the balance of forces in the oil/water/pipe surface system [16]:

(3)

A hydrocarbon-metal interface is replaced by water-metal interface favorably in energy decrease energy decrease of the system. Figure 6 shows water wettability of pipe surface decreases as water contact angles decrease; and it is assumed from the experimental observations that the water-pipe surface tension does not change for a pipe material. From Eq. 3, with heavy hydrocarbons, oil-water surface tension and/or oil-pipe surface tension become lower, decreasing water wettability, and repulsion of water by oil on pipe surface provides protection against corrosion. To determine whether the surface is oil-wet, mixed-wet or water-wet, the angle at the oil-water-surface intersection is observed and measured. Sequence of adding liquid phases to the surface could be oil first and then water or vice versa; then either the exterior or interior contact angle is measured. Such measurement is illustrated in Figure 6, which shows oil-first-water-second sequence and determination of exterior contact angle. The wettability of surface to oil and water is categorized in Table 1.

Table 1. Methods for measuring and reporting contact angles [2]

4. Corrosivity of aqueous phase in crude oil

Corrosion in oil pipelines initiates from water and the dissolved salts and gases in oils. Corrosivity of the aqueous phase depends on the composition of the electrolyte (the water phase), the contents and amounts of dissolved gases, pH, pressure, and temperature. The corrosiveness of the aqueous phase in the presence of oil can be determined by methods described in ASTM standards D665, G170, G184, G202, and NACE standard TM0172.

4.1. Composition of the aqueous phase in hydrocarbon fluids

Water fractions in crude oil could be as high as 10% in upstream gathering lines. Although separators remove water from oil before pumping through transmission pipelines, small amounts of water (as little as 0.5%) could remain as micro-droplets. Methods to determine water amounts in oil are described in ASTM D4006 and ASTM D4007 standards. The water droplets could coalesce and settle at the bottom of the pipeline, forming the water phase, flowing in different patterns controlled by the hydrodynamics of the pipeline flow. Water settling enhances by solid sediments in oils that are usually encapsulated by water and are more ready to go to bottom than water droplets. Water settlement does not occur uniformly along the pipeline but rather localized, at favorable hydrodynamic locations. Large fractions of water could accumulate at some segments of the pipeline, making corrosion far from uniform, occurring at difficult-to-predict locations.

The composition of the aqueous phase in oil-water mixtures is usually complex with numerous organic and inorganic constituents [17]. The amounts of inorganic salts in crude oil varies according to the geologic formation, and can be as high as 200,000 ppm [18]. They also are influenced by the oil-recovery techniques, which involve introducing water or steam into the formation. Typical constituents found in oilfield brines are summarized in Table 2 [19].

Table 2. Typical constituents found in oilfield brines [19]

The chemical composition of salts varies, and the major portion is nearly always sodium chloride with lesser amounts of calcium and magnesium chlorides [20]. Bicarbonate, carbonate, and sulfate salts leached from the formation rocks are present in crude oil in trace amounts. ASTM G3230 provides a guideline for the determination of salt content in crude oil using electrometric method. Aqueous solutions of chlorides, sulfates, carbonates, and acetates can form highly conductive electrolyte which is the medium for corrosion to occur. In addition, these anions when dissociate in water can significantly reduce the pH of the electrolyte and hence increase the corrosivity of the aqueous phase. At temperatures above 120oC, chloride salts break down to hydrochloric acid, an extremely corrosive constituent, as:

CaCl2 + H2O → CaO + 2HCl		 (4)

Presence of chloride salts in crude oil causes serious problems for not only transmission pipelines but also for tubing and heat exchangers in refineries.

4.2. O2 in hydrocarbon fluids

Oxygen can dissolve in hydrocarbon fluids wherever exposed to air, or air permeates into the pipes through leaks. Generally, the concentration of oxygen in crude oils is low because there is sufficient dissolved gases such as carbon dioxide and hydrogen sulfide at equilibrium that prevent oxygen dissolving at high concentration in oil. Hydrogen sulfide has high affinity to oxygen, reacting with it as:

2H2S + 3O2 → 2SO2 + 2H2O     (5)

This further reduces oxygen concentration in oil in the presence of hydrogen sulfide. In oil-water mixture, oxygen dissolves unequally into the two phases of which oil captures more oxygen than water due to the higher solubility of oxygen in oil. For instance, a water stream saturated with oxygen at 8 ppm will contain only 40 ppb oxygen after mixing with oil in a mixture of 0.5% water [21]. Influence of oxygen on pipe corrosion is strongest near the inlet where oxygen enters the pipeline, and it decreases downstream as oxygen gradually dissolves in the mixture, and it gets consumed in corrosion reactions.

4.3. CO2 in hydrocarbon fluids

Carbon dioxide in crude oils is from three different sources; (i) naturally trapped in oil formation, (ii) by-product of oil extraction process using strong acids such as HCl, HF and formic acid to stimulate sedimentary rocks, and (iii) being injected into oil wells for enhanced oil recovery. Carbon dioxide is highly soluble in water and it forms the corrosive carbonic acid. Carbonic acid dissociates to bicarbonate and carbonate, which enhance the cathodic reactions, hence increasing the corrosion rates. The presence of carbon dioxide also increases hydrogen evolution, which contributes to higher susceptibility to hydrogen embrittlement and catastrophic failures in pipelines.

4.4 Sulfur and H2S in hydrocarbon fluids

Sulfur in crude oil forms organic bonds with hydrocarbon compounds, and small amount of sulfur in form of free hydrogen sulfide dissolves in crude oil. Total sulfur content in crude oil varies from less than 0.1 to over 5% by weight [22]. Thermal decomposition of organic sulfur compounds, such as disulfides, thiols, aliphatic sulfides, and thiophenic compounds, adds to the content of hydrogen sulfide in oil [23-26]. Hydrogen sulfide could be produced by thermolysis of crude oils inside the formation where steam is injected into the well to enhance oil recovery, or in refineries where oil undergoes different cracking processes. Hydrogen sulfide could form as a result of microbial activities in the formation or inside pipelines [27-31]. Hydrogen sulfide is more soluble in water than carbon dioxide; forming weak acid and increasing corrosion rates of steels. The presence of HS- and S2- ions poisons the recombination reaction of H atoms to form H2 gas, hence more H atoms could ingress into the pipe materials and cause hydrogen embrittlement. This problem is referred to as sulfide stress corrosion cracking of pipelines.

5. Influence of oil chemistry on the corrosivity of the aqueous phase

Dissolution of ingredients from oil such as dissolved gases and organic compounds alters the corrosiveness of the aqueous phase. The origin of dissolved gases in oils and their corrosive effects is discussed in section 4; and this section focuses on the influence of organic compounds dissolved from crude oils on the corrosivity of the aqueous phase. The effects could be classified as corrosive, neutral, inhibitory, or preventive in nature [2]. Oil chemistry is complex and the exact composition of crude oil varies from field to field. So far, there is no systematic study on the influence of individual organic compound in crude oils on the corrosivity of the aqueous phase. Nevertheless it is well known that some organic compounds such as acetic acid increases the corrosion rates of steel [19, 32-34]. Conversely, other organic acids such as myristic or naphthenic acids were reported to inhibit corrosion in steel pipes [35-37]. Similar inhibition effect on uniform corrosion as well as sulfide stress corrosion cracking in steel was also observed, by saturate, aromatic and resin fractions separated from crude oils [38-41]. Absorption of surface active compounds creating organic films was proposed to account for the inhibition effect of crude oils [42, 43]. Accumulation of organic compounds on iron surfaces was observed by quartz microbalance and surface analytical techniques [44-46]. Modification of surface tension at the metal surface and at the oil-water interface in the presence of organic films that change the wettability of the metal surface inhibits corrosion [44, 47]. Absorbed organic films could change the flow pattern adjacent to the metal surface and facilitate water removal from the surface [36, 44].

6. Conclusion

- Corrosivity of oils containing water is determined by three factors: type of emulsion of oil and water, wettability of metal surface, and corrosivity of water phase.

- Water and oil are immiscible and they form different flow patterns during pipeline transportation that depends on: oil-to-water ratio, velocity of each phase, viscosity of oil, and geometrical factors.

- Water wettability of pipe surface decreases as water contact angles decreases.

- With heavy hydrocarbons, oil-water surface tension and/or oil-pipe surface tension become lower, decreasing water wettability, and repulsion of water by oil on pipe surface provides protection against corrosion.

- Corrosivity of the aqueous phase depends on the composition of the electrolyte, the contents and amounts of dissolved gases, pH, pressure, and temperature.

References

1.	Roussak, O.V. and Gesser, H.D., "Applied chemistry : a textbook for engineers and technologists," Second edition. ed. xxiv, 372 pages.

2.	ASTM, "ASTM G205-10: Standard Guide for Determining Corrosivity of Crude Oils," ASTM International, West Conshohocken, PA, 2010.

3.	Flores, J.G., Chen, X.T., Sarica, C. and Brill, J.P., "Characterization of Oil-Water Flow Patterns in Vertical and Deviated Wells," SPE Production & Facilities, Vol. 14(2), 1999.

4.	Elseth, G., "An experimental study of oil/water flow in horizontal pipes," Department of Technology (HiT-TF), Telemark University College, 2001.

5.	Trallero, J. and Brill, J., "A study of oil/water flow patterns in horizontal pipes," SPE Production and Facilities, Vol. 12(3), 1997, pp. 165-172.

6.	Rodriguez, O.M.H. and Oliemans, R.V.A., "Experimental study on oil–water flow in horizontal and slightly inclined pipes," International Journal of Multiphase Flow, Vol. 32(3), 2006, pp. 323-343.

7.	Baker, O., "Design of Pipelines for the Simultaneous Flow of Oil and Gas," Fall Meeting of the Petroleum Branch of AIME, 19-21 October, Dallas, TX, Society of Petroleum Engineers.

8.	Coleman, J.W. and Garimella, S., "Characterization of two-phase flow patterns in small diameter round and rectangular tubes," International Journal of Heat and Mass Transfer, Vol. 42(15), 1999, pp. 2869-2881.

9.	Lovick, J. and Angeli, P., "Experimental studies on the dual continuous flow pattern in oil–water flows," International journal of multiphase flow, Vol. 30(2), 2004, pp. 139-157.

10.	Arirachakaran, S., Oglesby, K.D., Malinowsky, M.S., Shoham, O. and Brill, J.P., "An Analysis of Oil/Water Flow Phenomena in Horizontal Pipes," SPE Production Operations Symposium, 13-14 March, Oklahoma City, OK, Society of Petroleum Engineers.

11.	Brauner, N. and Ullmann, A., "Modeling of phase inversion phenomenon in two-phase pipe flows," International Journal of Multiphase Flow, Vol. 28(7), 2002, pp. 1177-1204.

12.	Brooks, B. and Richmond, H., "Phase inversion in non-ionic surfactant—oil—water systems—II. Drop size studies in catastrophic inversion with turbulent mixing," Chemical engineering science, Vol. 49(7), 1994, pp. 1065-1075.

13.	Brooks, B.W. and Richmond, H.N., "Phase inversion in non-ionic surfactant—oil—water systems—I. The effect of transitional inversion on emulsion drop sizes," Chemical engineering science, Vol. 49(7), 1994, pp. 1053-1064.

14.	Brooks, B. and Richmond, H., "Phase inversion in non-ionic surfactant—oil—water systems—III. The effect of the oil-phase viscosity on catastrophic inversion and the relationship between the drop sizes present before and after catastrophic inversion," Chemical engineering science, Vol. 49(11), 1994, pp. 1843-1853.

15.	Nädler, M. and Mewes, D., "Flow induced emulsification in the flow of two immiscible liquids in horizontal pipes," International Journal of Multiphase Flow, Vol. 23(1), 1997, pp. 55-68.

16.	Glasstone, S., "Textbook of physical chemistry," 2d ed. New York,, D. Van Nostrand company, 1946, xiii, 1320 pages.

17.	Fortuny, M., Silva, E.B., Agnaldo Filho, C., Melo, R.L., Nele, M., Coutinho, R.C. and Santos, A.F., "Measuring Salinity in crude oils: Evaluation of methods and an improved procedure," Fuel, Vol. 87(7), 2008, pp. 1241-1248.

18.	Mohamed, A.-M.O., El Gamal, M. and Zekri, A.Y., "Effect of salinity and temperature on water cut determination in oil reservoirs," Journal of Petroleum Science and Engineering, Vol. 40(3–4), 2003, pp. 177-188.

19.	Nešić, S., "Key issues related to modelling of internal corrosion of oil and gas pipelines – A review," Corrosion Science, Vol. 49(12), 2007, pp. 4308-4338.

20.	Fortuny, M., Oliveira, C.B.Z., Melo, R.L.F.V., Nele, M., Coutinho, R.C.C. and Santos, A.F., "Effect of Salinity, Temperature, Water Content, and pH on the Microwave Demulsification of Crude Oil Emulsions†," Energy & Fuels, Vol. 21(3), 2007, pp. 1358-1364.

21.	"State of the Art Report-Dilbit Corrosivity," Canadian Energy Pipelines Association, Penspen Integrity, Richmond Upon Thames, UK, 2013.

22.	Harry, G. and Clifford, M., "ASTM MNL68 Handbook: Crude Oils: Their Sampling, Analysis, and Evaluation," West Conshohocken, PA, ASTM International, 2010.

23.	Clark, P.D. and Hyne, J.B., "Chemistry of organosulphur compound types occurring in heavy oil sands: 3. Reaction of thiophene and tetrahydrothiophene with vanadyl and nickel salts," Fuel, Vol. 63(12), 1984, pp. 1649-1654.

24.	Ritchie, R.G.S., Roche, R.S. and Steedman, W., "Non-isothermal programmed pyrolysis studies of oil sand bitumens and bitumen fractions: 1. Athabasca asphaltene," Fuel, Vol. 64(3), 1985, pp. 391-399.

25.	Clark, P.D., Hyne, J.B. and Tyrer, J.D., "Chemistry of organosulphur compound types occurring in heavy oil sands:: 1. High temperature hydrolysis and thermolysis of tetrahydrothiophene in relation to steam stimulation processes," Fuel, Vol. 62(8), 1983, pp. 959-962.

26.	Orr, W.L., "Changes in Sulfur Content and Isotopic Ratios of Sulfur during Petroleum Maturation; Study of Big Horn Basin Paleozoic Oils," AAPG Bulletin, Vol. 58(11 Part 1), 1974, pp. 2295-2318.

27.	Nemati, M., Jenneman, G.E. and Voordouw, G., "Mechanistic study of microbial control of hydrogen sulfide production in oil reservoirs," Biotechnology and Bioengineering, Vol. 74(5), 2001, pp. 424-434.

28.	Cord-Ruwisch, R., Kleinitz, W. and Widdell, F., "Sulfate-reducing bacteria and their activities in oil production," J. Pet. Technol., Vol. 39(1), 1987, pp. 97-106.

29.	Tang, K., Baskaran, V. and Nemati, M., "Bacteria of the sulphur cycle: an overview of microbiology, biokinetics and their role in petroleum and mining industries," Biochemical Engineering Journal, Vol. 44(1), 2009, pp. 73-94.

30.	Youssef, N., Elshahed, M.S. and McInerney, M.J., "Microbial processes in oil fields: culprits, problems, and opportunities," Advances in applied microbiology, Vol. 66, 2009, pp. 141-251.

31.	Magot, M., Ollivier, B. and Patel, B.C., "Microbiology of petroleum reservoirs," Antonie van Leeuwenhoek, Vol. 77(2), 2000, pp. 103-116.

32.	Ajayi, F. and Lyon, S., "Detrimental Effects of Acetic Acid on Corrosion of Carbon Steel Pipelines Transporting Wet Gas," SPE Nigeria Annual International Conference and Exhibition, 5-7 August, Lagos, Nigeria, Society of Petroleum Engineers.

33.	Singer, M., Brown, B., Camacho, A. and Nesic, S., "Combined effect of CO2, H2S and acetic acid on bottom of the line corrosion," CORROSION 2007, 11-15 March, Nashville, TN, NACE International.

34.	Sun, Y., George, K. and Nesic, S., "The Effect of Cl- and Acetic Acid on Localized CO2 Corrosion in Wet Gas Flow," CORROSION 2003, 16-20 March, San Diego, CA, 2003, NACE International.

35.	Migahed, M. and Al-Sabagh, A., "Beneficial role of surfactants as corrosion inhibitors in petroleum industry: a review article," Chemical Engineering Communications, Vol. 196(9), 2009, pp. 1054-1075.

36.	Ayello, F., Robbins, W., Richter, S. and Nešic, S., "Model Compound Study of the Mitigative Effect of Crude Oil on Pipeline Corrosion," Corrosion, Vol. 69(3), 2012, pp. 286-296.

37.	Papavinasam, S., Revie, R., Attard, M., Demoz, A. and Michaelian, K., "Comparison of laboratory methodologies to evaluate corrosion inhibitors for oil and gas pipelines," Corrosion, Vol. 59(10), 2003, pp. 897-912.

38.	Mendez, C., Dupla, S., Hernandez, S. and Vera, J.R., "On the Mechanism of Corrosion Inhibition by Crude Oils," CORROSION 2001, 11-16 March, NACE International, Houston, TX, 2001

39.	Rocha Junior, L.C., Ferreira, M.S. and da Silva Ramos, A.C., "Inhibition of asphaltene precipitation in Brazilian crude oils using new oil soluble amphiphiles," Journal of Petroleum Science and Engineering, Vol. 51(1–2), 2006, pp. 26-36.

40.	Khalifa, M.A., El-Batouti, M., Mahgoub, F. and Bakr Aknish, A., "Corrosion inhibition of steel in crude oil storage tanks," Materials and Corrosion, Vol. 54(4), 2003, pp. 251-258.

41.	Yang, S., Richter, S., Robbins, W. and Nesic, S., "Evaluation of the Protectiveness of a Paraffin Layer In CO2 Corrosion of Mild Steel," CORROSION 2012, 11-15 March, Salt Lake, UT, 2012, NACE International.

42.	Efird, K.D. and Jasinski, R.J., "Effect of the Crude Oil on Corrosion of Steel in Crude Oil/Brine Production," Corrosion, Vol. 45(2), 1989, pp. 165-171.

43.	Hernández, S., Nešić, S., Weckman, G. and Ghai, V., "Use of artificial neural networks for predicting crude oil effect on carbon dioxide corrosion of carbon steels," Corrosion, Vol. 62(6), 2006, pp. 467-482.

44.	Ayello, F., Robbins, W., Richter, S. and Nesic, S., "Crude oil chemistry effects on inhibition of corrosion and phase wetting," 17th Int. Corros. Cong., paper, (3149), 2011.

45.	Rudrake, A., Karan, K. and Horton, J.H., "A combined QCM and XPS investigation of asphaltene adsorption on metal surfaces," Journal of colloid and interface science, Vol. 332(1), 2009, pp. 22-31.

46.	Balabin, R.M., Syunyaev, R.Z., Schmid, T., Stadler, J., Lomakina, E.I. and Zenobi, R., "Asphaltene adsorption onto an iron surface: combined near-infrared (NIR), Raman, and AFM study of the kinetics, thermodynamics, and layer structure," Energy & Fuels, Vol. 25(1), 2010, pp. 189-196.

47.	Carlos da Silva Ramos, A., Haraguchi, L., Notrispe, F.R., Loh, W. and Mohamed, R.S., "Interfacial and colloidal behavior of asphaltenes obtained from Brazilian crude oils," Journal of Petroleum Science and Engineering, Vol. 32(2–4), 2001, pp. 201-216.